Supporting information

Predictive and Interpretable Data-Driven Framework for Deciphering Chiral Emergence of Conjugated Polymers

Sanghyun Jeon1,†, Hang Zhang2,†, Nahyun Ahn3, Ayse Senlik3, Rui Zhang3, Yejin Shim3, Janice Baek1, Priyotosh Bairagya3, Pravini S. Fernando3, Justine Wagner4,5,6, Justin Scott Neu7, Duyen Tran8, Kousseff Christina9, Anna M. Österholm10, Samson A. Jenekhe8, Iain McCulloch9, Wei You7, John R. Reynolds10, Nicholas E. Jackson1,2,3,11,*, Ying Diao1,2,3,11,*

1Department of Materials Science and Engineering, University of Illinois Urbana−Champaign, 600 S. Mathews Avenue, Urbana, Illinois 61801, United States

2Department of Chemistry, Department of Materials Science and Engineering, University of Illinois Urbana−Champaign, 600 S. Mathews Avenue, Urbana, Illinois 61801, United States

3Department of Chemical and Biomolecular Engineering, University of Illinois Urbana−Champaign, 600 S. Mathews Avenue, Urbana, Illinois 61801, United States

4School of Chemistry and Biochemistry, Center for Organic Photonics and Electronics, Georgia Institute of Technology, Atlanta, Georgia, 30332, United States.

5 Materials and Manufacturing Directorate, Air Force Research Laboratory, Wright-Patterson Air Force Base, Dayton, Ohio, 45433, United States.

6 AV, Inc., Beavercreek, Ohio, 45432, United States.

7Department of Chemistry, University of North Carolina, Chapel Hill, North Carolina 27599, United States

8Department of Chemical Engineering and Department of Chemistry, University of Washington, Seattle, Washington 98195, United States

9Department of Chemistry, University of Oxford, Oxford, United Kingdom

10School of Chemistry and Biochemistry, School of Materials Science and Engineering, Georgia Institute of Technology, Atlanta, Georgia 30322, United States

11Beckman Institute for Advanced Science and Technology, University of Illinois Urbana−Champaign, Urbana, Illinois 61801, United States

†These authors contributed equally to this work.

For correspondence: yingdiao@illinois.edu, jacksonn@illinois.edu

Table of Contents

Section S1. Experimental Details for Chirality Measurements, Dataset Construction, and Material synthesis	8

Section S2. Details on features considered in this study.	73

Section S3. Selection of machine-learning framework.	74

Section S4. Family related RF classification model performance.	77

Section S5. Solubility-based evidence supporting the proposed mechanism of chiral LLC formation.	80

Section S6. Additional results for feature analysis.	85

List of Supporting Figures

Figure S1. Four-scan method for extraction of the true CD signal from aligned LLC samples. (a) Schematic illustration of the measurement geometry.	11

Figure S2. Spectral regions used to distinguish intrinsic CD from artifact-dominated signals and to evaluate the dissymmetry factor.	13

Figure S3. 1H NMR spectrum of 2,5-dibromo-3,4-ethylenedixoythiophene [dibromo-EDOT].	24

Figure S4. 13C NMR spectrum of 2,5-dibromo-3,4-ethylenedixoythiophene [dibromo-EDOT].	25

Figure S5. 1H NMR spectrum of 2,2’,3,3’-tetrahydro-5,5’-bithieno[3,4-b][1,4]dioxine [Bi-EDOT].	26

Figure S6. 13C NMR spectrum of 2,2’,3,3’-tetrahydro-5,5’-bithieno[3,4-b][1,4]dioxine [Bi-EDOT].	27

Figure S7. 1H NMR spectrum of 7,7‘-dibromo-2,2‘,3,3‘-tetrahydro-5,5‘-bithieno[3,4-b][1,4]dioxine [dibromo Bi-EDOT].	28

Figure S8. 13C NMR spectrum of 7,7‘-dibromo-2,2‘,3,3‘-tetrahydro-5,5‘-bithieno[3,4-b][1,4]dioxine [dibromo Bi-EDOT].	29

Figure S9. 1H NMR spectrum of 7,7‘-bis(trimethylstannyl)2,2‘,3,3‘-tetrahydro-5,5‘-bithieno[3,4-b][1,4]dioxine [Bis-trimethyltin Bi-EDOT].	30

Figure S10. 13C NMR spectrum of 7,7‘-bis(trimethylstannyl)2,2‘,3,3‘-tetrahydro-5,5‘-bithieno[3,4-b][1,4]dioxine [Bis-trimethyltin Bi-EDOT].	31

Figure S11. 1H NMR spectrum of 1,4-bis(octyloxy)benzene.	32

Figure S12. 13C NMR spectrum of 1,4-bis(octyloxy)benzene.	33

Figure S13. 1H NMR spectrum of 1,4-dibromo-2,5-bis(octyloxy)benzene.	34

Figure S14. 13C NMR spectrum of 1,4-dibromo-2,5-bis(octyloxy)benzene.	35

Figure S15. 1H NMR spectrum of triethylene glycol monomethyl ether tosylate.	36

Figure S16. 13C NMR spectrum of triethylene glycol monomethyl ether tosylate.	37

Figure S17. 1H NMR spectrum of 1,4-dibromo-2,5-bis(2-(2-(2 methoxyethoxy)ethoxy)ethoxy) benzene.	38

Figure S18. 13C NMR spectrum of 1,4-dibromo-2,5-bis(2-(2-(2 methoxyethoxy)ethoxy)ethoxy) benzene.	39

Figure S19. 1H NMR spectrum of 3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophene.	40

Figure S20. 13C NMR spectrum of 3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophene.	41

Figure S21. 1H NMR spectrum of Triisopropyl(3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy) thiophen-2-yl)silane.	42

Figure S22. 13C NMR spectrum of Triisopropyl(3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy) thiophen-2-yl)silane.	43

Figure S23. 1H NMR spectrum of 2-(4-decylthiophen-2-yl)-4,4,5,5-tetramethyl-1,3,2-dioxaborolane.	44

Figure S24. 13C NMR spectrum of 2-(4-decylthiophen-2-yl)-4,4,5,5-tetramethyl-1,3,2-dioxaborolane.	45

Figure S25. 1H NMR spectrum of 5,5’-(2,5’bis(octyloxy)-1,4-phenylene)bis(3-decylthiophene) (TPT C10/C8).	46

Figure S26. 13C NMR spectrum of 5,5’-(2,5’bis(octyloxy)-1,4-phenylene)bis(3-decylthiophene) (TPT C10/C8).	47

Figure S27. 1H NMR spectrum of 5,5’-(2,5’bis(octyloxy)-1,4-phenylene)bis(2-bromo3-decylthiophene) (dibromo TPT C10/C8).	48

Figure S28. 13C NMR spectrum of 5,5’-(2,5’bis(octyloxy)-1,4-phenylene)bis(2-bromo3-decylthiophene) (dibromo TPT C10/C8).	49

Figure S29. 1H NMR spectrum of ((2,5-bis(octyloxy)-1,4-phenylene)bis(3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophene-5,2-diyl))bis(triisopropylsilane) TIPS-(T(OE3)P(OC8).	50

Figure S30. 13C NMR spectrum of ((2,5-bis(octyloxy)-1,4-phenylene)bis(3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophene-5,2-diyl))bis(triisopropylsilane) TIPS-(T(OE3)P(OC8).	51

Figure S31. 1H NMR spectrum of 5,5’-(2,5-bis(octyloxy)-1,4-phenylene)bis(3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophene) [H-T(OE3)P(OC8)-H].	52

Figure S32. 13C NMR spectrum of 5,5’-(2,5-bis(octyloxy)-1,4-phenylene)bis(3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophene) [H-T(OE3)P(OC8)-H].	53

Figure S33. 1H NMR spectrum of ((2,5-bis(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)-1,4-phenylene)bis(3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophene-5,2-diyl))bis(triisopropylsilane) TIPS-T(OE3)P(OE3).	54

Figure S34. 13C NMR spectrum of ((2,5-bis(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)-1,4-phenylene)bis(3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophene-5,2-diyl))bis(triisopropylsilane) TIPS-T(OE3)P(OE3).	55

Figure S35. 13C NMR spectrum of 5,5’-(2,5-bis(2-(2-(2-(methoxyethoxy)ethoxy)ethoxy)-1,4-phenylene)bis(3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophene) [H-T(OE3)P(OE3)-H].	56

Figure S36. 13C NMR spectrum of 5,5’-(2,5-bis(2-(2-(2-(methoxyethoxy)ethoxy)ethoxy)-1,4-phenylene)bis(3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophene) [H-T(OE3)P(OE3)-H].	57

Figure S37. 1H NMR spectrum of TPT-E (C8/C10).	58

Figure S38. 13C NMR spectrum of TPT-E (C8/C10).	59

Figure S39. Size exclusion chromatogram of TPT-E (C8/C10) in 40 °C CHCl3 (calibrated versus polystyrene standards).	59

Figure S40. 1H NMR spectrum of TPT-2E (C8/C10).	60

Figure S41. 13C NMR spectrum of TPT-2E (C8/C10).	61

Figure S42. Size exclusion chromatogram of TPT-2E (C8/C10) in 40 °C CHCl3 (calibrated versus polystyrene standards).	62

Figure S43. 1H NMR spectrum of T(OE3)P(OC8)-E.	63

Figure S44. 13C NMR spectrum of T(OE3)P(OC8)-E.	64

Figure S45. Size exclusion chromatogram of T(OE3)P(OC8)-E in 40 °C CHCl3 (calibrated versus polystyrene standards).	64

Figure S46. 1H NMR spectrum of T(OE3)P(OE3)-E.	65

Figure S47. 13C NMR spectrum of T(OE3)P(OE3)-E.	66

Figure S48. Size exclusion chromatogram of T(OE3)P(OE3)-E in 40 °C CHCl3 (calibrated versus polystyrene standards).	66

Figure S49. 1H-NMR spectrum (500 MHz) of ProDOT(OE3)-co-ProDOT(Oct) in CDCl3.	68

Figure S50. Size exclusion chromatogram of ProDOT(OE3)-co-ProDOT(Oct) (40 °C CHCl3, calibrated versus polystyrene).	68

Figure S51. Size exclusion chromatograms of PyDPP-2T polymer in 1,2,4-trichlorobenzen at 140 oC (calibrated vs. polystyrene).	70

Figure S52. Size exclusion chromatograms of PyDPP-2T2F polymer in 1,2,4-trichlorobenzen at 140 oC (calibrated vs. polystyrene).	71

Figure S53. 1H NMR spectrum of C10C12PyDPPBr at room temperature in CDCl3.	72

Figure S54. 13C NMR spectrum of C10C12PyDPPBr at room temperature in CDCl3.	73

Figure S55. MALDI-TOF spectrum of C10C12PyDPPBr.	74

Figure S56. Size exclusion chromatograms of C10C12PyDPP-2T polymer in 1,2,4-trichlorobenzene at 140 oC (calibrated vs. polystyrene).	75

Figure S57. Complete list of the 77 features considered in this study.	76

Figure S58. SHAP importance and importance-rank stability of the top 20 features for the RF classification model trained on the full polymer dataset.	79

Figure S59. Distributions of negative log∣g∣<-3 and positive log∣g∣≥-3 cases with respect to the polymer molecular weight used in the SHAP analysis of RF classification models trained on full processed ML dataset.	83

Figure S60. Experimental distribution of assembly outcome in the two-dimensional space defined by the FASTSOLV-derived monomer and backbone solubility descriptors.	84

Figure S61. Relationship between monomer FASTSOLV and assembly outcome.	85

Figure S62. RF prediction score of log⁡10∣g∣≥-3 in the two-dimensional space defined by the FASTSOLV-derived monomer and backbone solubility descriptors for the expanded polymer–solvent dataset.	86

Figure S63. Experimentally observed assembly outcomes plotted as a function of normalized side-chain content.	88

Figure S64. SHAP importance and importance-rank stability of the top 20 features for the RF classification model trained on the thiophene family subset.	89

Figure S65. SHAP importance and importance-rank stability of the top 20 features for the RF classification model trained on the NDI family subset.	90

Figure S66. Concentration-resolved experimental assembly outcomes for NDI-family polymers, including p(C3NDI-T), p(C6NDI-T), N2200-OE, and N2200 with six different molecular weights.	91

List of Supporting Tables

Table S1. Dataset used for machine-learning analysis.	11

Table S2. Comparison between ML frameworks on the classification task.	74

Table S3. Comparison between ML frameworks on the regression task.	74

Table S4. Results of leave-one-family-out evaluation.	77

Section S1. Experimental Details for Chirality Measurements, Dataset Construction, and Material synthesis

Figure S1. Four-scan method for extraction of the true CD signal from aligned LLC samples. (a) Schematic illustration of the measurement geometry. CD spectra were collected at four sample orientations defined by (θ, β) = (0°, 0°), (90°, 0°), (0°, 180°), and (90°, 180°), where θ and β denote the in-plane and out-of-plane rotation angles, respectively.

To extract the true circular dichroism signal (CDtrue) from aligned LLC samples, we employed the previously reported four-scan method1. This procedure separates the measured CD signal from contributions arising from linear dichroism/linear birefringence (CDLDLB) and residual static birefringence associated with the photoelastic modulator (CDα). CD spectra were collected at four sample orientations defined by the in-plane rotation angle, θ, and the out-of-plane rotation angle, β: (θ, β) = (0°, 0°), (90°, 0°), (0°, 180°), and (90°, 180°), and the true CD signal was obtained by averaging the four measurements:

CDtrue = [CD(θ=0°, β=0°) + CD(θ=90°, β=0°) + CD(θ=0°, β=180°) + CD(θ=90°, β=180°)] / 4

The CDLDLB contributions for the two out-of-plane orientations were calculated as:

CDLDLB, β=180° = [CD(θ=0°, β=180°) + CD(θ=90°, β=180°) − 2CDtrue] / 2

CDLDLB, β=0° = [CD(θ=0°, β=0°) + CD(θ=90°, β=0°) − 2CDtrue] / 2

Similarly, the CDα contributions for the two in-plane orientations were calculated as:

CDα, θ=90° = [CD(θ=90°, β=0°) + CD(θ=90°, β=180°) − 2CDtrue] / 2

CDα, θ=0° = [CD(θ=0°, β=0°) + CD (θ=0°, β=180°) − 2CDtrue] / 2

Thus, averaging the four measurements isolates the orientation-independent CDtrue component, while the remaining pairwise deviations provide estimates of the CDLDLB and CDα contributions.

Figure S2. Spectral regions used to distinguish intrinsic CD from artifact-dominated signals and to evaluate the dissymmetry factor. Representative g-factor, CD, and absorbance spectra are shown as a function of wavelength. The blue-shaded region denotes the absorption-active spectral range, where the CD response is attributed primarily to the intrinsic chiroptical response of the polymer assembly. The red-shaded region corresponds to wavelengths with negligible absorbance, where the observed CD signal is more likely dominated by anisotropy- or scattering-induced artifacts2. The g-factor was evaluated within the indicated wavelength region associated with the absorption-active CD response.

Table S1. Dataset used for machine-learning analysis.

Each entry lists the polymer, solvent, temperature, concentration, structural classification, and data origin. Samples were classified as chiral (c), isotropic (i), or aggregated (a), and the origin of each entry was identified as either literature-derived or generated in this work. For isotropic or aggregated samples tested over a concentration range of 100–300 mg/mL, the range is shown as a single entry in the table for simplicity. However, for machine-learning analysis, these conditions were treated as three separate data points corresponding to 100, 200, and 300 mg/mL. When multiple CD measurements were collected under the same experimental condition, each measurement was treated as an independent data point. For example, for p(g42T-TT) in chloroform at 25 °C and 100 mg/mL, two separate CD measurements were obtained and both exhibited CD signals; these were therefore counted as two independent data points in the ML dataset.

| Polymer [Source] | Solvent | Temp. | Conc. | Type | Data Source |
| --- | --- | --- | --- | --- | --- |
| p(g4(2T-TT)) [3] | Chloroform | 25 | 50mgmL | c | This work + DOI: 10.1002/adma.74130 |
|  |  |  | 100mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  | 200mgmL | c |  |
|  |  |  | 300mgmL | c |  |
|  | Anisole | 25 | 100-300mgmL | a |  |
|  |  | 50 | 100-300mgmL | a |  |
|  |  | 70 | 100-300mgmL | a |  |
|  |  | 90 | 300mgmL | c |  |
|  |  | 110 | 300mgmL | c |  |
|  |  | 130 | 300mgmL | c |  |
|  | o-dichlorobenzene | 25 | 100-300mgmL | a |  |
|  |  | 130 | 300mgmL | c |  |
|  |  |  |  | c |  |
|  | Chlorobenzene | 25 | 100-300mgmL | a |  |
|  | 1-Chloronaphthalene | 25 | 100-300mgmL | a |  |
|  |  | 130 | 300mgmL | c |  |
|  | Dimethylformamide | 25 | 100-300mgmL | a | This work |
|  | 14dioxane | 25 | 100-300mgmL | a |  |
|  | 13dioxane | 25 | 100-300mgmL | a |  |
|  | Trichloroethylene | 25 | 100-300mgmL | a | DOI: 10.1002/adma.74130 |
|  | Toluene | 25 | 100-300mgmL | a |  |
|  | o-xylene | 25 | 100-300mgmL | a | This work |
|  | p-xylene | 25 | 100-300mgmL | a | This work |
|  | Propylene Glycol Methyl Ether Acetate | 25 | 100-300mgmL | a | DOI: 10.1002/adma.74130 |
|  |  | 130 | 100-300mgmL | a |  |
|  | Ethanol | 25 | 100-300mgmL | a | This work |
| p(g3(2T-TT)) [3] | Chloroform | 25 | 300mgmL | c | This work + DOI: 10.1002/adma.74130 |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  | Anisole | 25 | 100-300mgmL | a |  |
|  |  | 130 | 200mgmL | c |  |
|  | o-dichlorobenzene | 25 | 100-300mgmL | a |  |
|  |  | 130 | 200mgmL | c |  |
|  | Chlorobenzene | 25 | 100-300mgmL | a | This work |
|  | Dimethylformamide | 25 | 100-300mgmL | a |  |
|  | 1-Chloronaphthalene | 25 | 100-300mgmL | a |  |
|  | 14dioxane | 25 | 100-300mgmL | a |  |
|  | 13dioxane | 25 | 100-300mgmL | a |  |
|  | Trichloroethylene | 25 | 100-300mgmL | a |  |
|  | Toluene | 25 | 100-300mgmL | a |  |
|  | o-xylene | 25 | 100-300mgmL | a |  |
|  | p-xylene | 25 | 100-300mgmL | a |  |
|  | Propylene Glycol Methyl Ether Acetate | 25 | 100-300mgmL | a |  |
|  |  | 130 | 100-300mgmL | a |  |
|  | Ethanol | 25 | 100-300mgmL | a |  |
| p(g3(2T-T)) [3] | Chloroform | 25 | 300mgmL | c | This work + DOI: 10.1002/adma.74130 |
|  |  |  |  | c |  |
|  | Anisole | 25 | 200mgmL | c |  |
|  | o-dichlorobenzene | 25 | 200mgmL | c |  |
|  | Propylene Glycol Methyl Ether Acetate | 25 | 100-300mgmL | a | This work + DOI: 10.1002/adma.74130 |
|  |  | 130 | 200mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  | Ethanol | 25 | 100-300mgmL | a |  |
|  | Chlorobenzene | 25 | 300mgmL | c |  |
|  | 1-Chloronaphthalene | 25 | 300mgmL | c |  |
|  | Dimethylformamide | 25 | 300mgmL | c |  |
|  | Trichloroethylene | 25 | 300mgmL | c |  |
|  | Toluene | 25 | 300mgmL | c |  |
|  | p-xylene | 25 | 300mgmL | i |  |
| PBTTT-OE3 [3] | Chloroform | 25 | 100mgmL | c | This work + DOI: 10.1002/adma.74130 |
|  |  |  | 200mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  | 300mgmL | c |  |
|  |  |  |  | c |  |
|  | Anisole | 25 | 100-300mgmL | a | DOI: 10.1002/adma.74130 |
|  | Propylene Glycol Methyl Ether Acetate | 25 | 100-300mgmL | a | This work |
|  | Ethanol | 25 | 100-300mgmL | a |  |
| PBTTT-C14 [3] | Chloroform | 25 | 100-300mgmL | a | This work |
|  | Anisole | 25 | 100-300mgmL | a |  |
|  |  | 130 | 100-300mgmL | i |  |
|  | o-dichlorobenzene | 25 | 100-300mgmL | i |  |
|  |  | 130 | 100-300mgmL | i |  |
|  | chlorobenzene | 25 | 100-300mgmL | a |  |
|  |  | 80 | 100-300mgmL | i |  |
|  | Dimethylformamide | 25 | 100-300mgmL | a |  |
|  |  | 130 | 100-300mgmL | a |  |
|  | 1-Chloronaphthalene | 25 | 100-300mgmL | a |  |
|  | Propylene Glycol Methyl Ether Acetate | 25 | 100-300mgmL | a |  |
|  |  | 130 | 100-300mgmL | a |  |
|  | 1,4-Dioxane | 25 | 100-300mgmL | a |  |
|  |  | 70 | 100-300mgmL | a |  |
|  | Trichloroethylene | 25 | 100-300mgmL | i |  |
|  | Toluene | 25 | 100-300mgmL | a |  |
|  | Ethanol | 25 | 100-300mgmL | a |  |
| P3HT [Sigma-Aldrich] | Chloroform | 25 | 100-300mgmL | i | This work |
|  | Chlorobenzene | 25 | 100-300mgmL | i |  |
|  | Trichlorobenzene | 25 | 100-300mgmL | i |  |
|  | Toluene | 25 | 100-300mgmL | a |  |
|  | o-dichlorobenzene | 25 | 100-300mgmL | i |  |
|  | Anisole | 25 | 100-300mgmL | a |  |
|  | 1-Chloronaphthalene | 25 | 100-300mgmL | i |  |
|  | Dimethylformamide | 25 | 100-300mgmL | a |  |
|  | p-xylene | 25 | 100-300mgmL | a |  |
|  | Ethanol | 25 | 100-300mgmL | a |  |
|  | Propylene Glycol Methyl Ether Acetate | 25 | 100-300mgmL | a |  |
| P3MEEMT [4] | Chloroform | 25 | 300mgmL | c | This work |
|  | Propylene Glycol Methyl Ether Acetate | 25 | 100-300mgmL | a |  |
| AcDOT-[C10]2-co-[OE3]2 [5] | Chloroform | 25 | 10mgmL | i | DOI:10.1021/10.1021/jacs.5c07995 |
|  |  |  | 50mgmL | i |  |
|  |  |  | 100mgmL | c |  |
|  |  |  | 200mgmL | c |  |
|  | Methanol | 25 | 100-300mgmL | a | This work |
|  | Chloroform (75wt%) + Methanol (25wt%) | 25 | 100-150mgmL | a |  |
| AcDOT-[CH3,C10]-co-[CH3,OE3] [6] | Chloroform | 25 | 100-300mgmL | i | DOI:10.1021/acs.chemmater.4c03394 |
| AcDOT-[C3-C10] [6] | Chloroform | 25 | 100-300mgmL | a | This work |
| AcDOT-[OE3]2 [6] | Chloroform | 25 | 100-300mgmL | a |  |
| AcDOT-[C10]2 [6] | Chloroform | 25 | 100-300mgmL | i | DOI:10.1021/acs.chemmater.4c03394 |
| PTQ-10 [5] | Chloroform | 25 | 100-300mgmL | i | This work |
|  | Chlorobenzene | 25 | 100-300mgmL | i |  |
| PTQ-2bO2 [5] | Chloroform | 25 | 100-300mgmL | i | This work |
|  |  | 50 | 100-300mgmL | i |  |
|  | Anisole | 25 | 100-300mgmL | a |  |
|  |  | 130 | 100-300mgmL | a |  |
|  | o-dichlorobenzene | 25 | 100-300mgmL | a |  |
|  |  | 130 | 100-300mgmL | i |  |
|  | Chlorobenzene | 25 | 10-200mgmL | a | DOI:10.1021/10.1021/jacs.5c07995 |
| PTQ-4bO2 [5] | Chloroform | 25 | 200mgmL | c | DOI: 10.1002/adma.74130 |
|  | chlorobenzene | 25 | 100mgmL | i | DOI:10.1021/10.1021/jacs.5c07995 |
|  |  |  | 150mgmL | c |  |
|  |  |  | 200mgmL | c |  |
|  |  |  | 300mgmL | c |  |
|  |  |  |  | c |  |
|  | o-dichlorobenzene | 25 | 100-300mgmL | i | DOI: 10.1002/adma.74130 |
|  |  | 100 | 200mgmL | c |  |
|  | 70% chlorobenzene + 30% Methanol | 25 | 40mgmL | i | This work |
|  |  |  | 70mgmL | i |  |
|  |  |  | 100mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  | 150mgmL | c |  |
|  | 30% chlorobenzene + 70% Methanol | 25 | 100-300mgmL | a |  |
| PTQ-6bO [3] | Chloroform | 25 | 200mgmL | c | DOI: 10.1002/adma.74130 |
|  | o-dichlorobenzene | 25 | 100-300mgmL | a |  |
|  |  | 100 | 200mgmL | c |  |
|  | Anisole | 25 | 100-300mgmL | a |  |
|  |  | 100 | 200mgmL | c |  |
|  | Propylene Glycol Methyl Ether Acetate | 25 | 100-300mgmL | a |  |
|  |  | 130 | 100-300mgmL | a |  |
| PTQ-6O [5] | Chlorobenzene | 25 | 10-300mgmL | a | DOI:10.1021/10.1021/jacs.5c07995 |
| PTQ-6bO2 [5] | chlorobenzene | 25 | 100mgmL | c | DOI:10.1021/10.1021/jacs.5c07995 |
|  |  |  | 200mgmL | c |  |
|  |  |  | 250mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  | 300mgmL | c |  |
| N2200 - 3.6 k [5] | Chlorobenzene | 25 | 100-300mgmL | i | DOI:10.1021/10.1021/jacs.5c07995 |
| N2200 - 5.7 k [5] | Chlorobenzene | 25 | 100-300mgmL | i | DOI:10.1021/10.1021/jacs.5c07995 |
|  | Chloroform | 25 | 100-300mgmL | i | This work |
|  | Anisole | 25 | 100-300mgmL | i |  |
| N2200 - 9.1 k [5] | Chloroform | 25 | 50mgmL | c | This work + DOI:10.1021/10.1021/jacs.5c07995 |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 100mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 200mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  | chlorobenzene | 25 | 50mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 100mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 200mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 300mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  | o-dichlorobenzene | 25 | 50mgmL | c | This work |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 100mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 200mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  | Toluene | 25 | 50mgmL | i |  |
|  |  |  |  | i |  |
|  |  |  |  | c |  |
|  |  |  | 100mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 200mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  | p-xylene | 25 | 50mgmL | i |  |
|  |  |  |  | i |  |
|  |  |  |  | c |  |
|  |  |  | 100mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 200mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  | Anisole | 25 | 50mgmL | i |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 100mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 200mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
| N2200 - 22.0 k [5] | Chlorobenzene | 25 | 10mgmL | i | This work + DOI:10.1021/10.1021/jacs.5c07995 |
|  |  |  | 70mgmL | c |  |
|  |  |  | 100mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  | 150mgmL | c |  |
|  |  |  | 200mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 300mgmL | c |  |
| N2200 - 50.0 k [5] | Chlorobenzene | 25 | 10mgmL | i | DOI:10.1021/10.1021/jacs.5c07995 |
|  |  |  | 100mgmL | c |  |
|  |  |  | 150mgmL | c |  |
|  |  |  | 200mgmL | c |  |
|  |  |  | 300mgmL | c |  |
|  | o-dichlorobenzene | 25 | 300mgmL | c | This work |
|  | tetrachloroethylene | 25 | 300mgmL | c |  |
| N2200 - 130.0 k [5] | Chlorobenzene | 25 | 10mgmL | i | DOI:10.1021/10.1021/jacs.5c07995 |
|  |  |  | 30mgmL | i |  |
|  |  |  | 50mgmL | c |  |
|  |  |  | 100mgmL | c |  |
|  |  |  | 150mgmL | c |  |
|  |  |  | 200mgmL | c |  |
| N2200-OE [3] | Chloroform | 25 | 200mgmL | c | DOI: 10.1002/adma.74130 |
|  |  |  |  | c |  |
|  | Anisole | 25 | 100-300mgmL | a |  |
|  |  | 70 | 200mgmL | c |  |
|  | Chlorobenzene | 25 | 300mgmL | c | This work |
|  | o-dichlorobenzene | 25 | 300mgmL | c |  |
|  | Toluene | 25 | 100-300mgmL | a |  |
|  | p-xylene | 25 | 100-300mgmL | a |  |
|  | tetrachloroethylene | 25 | 100-300mgmL | a |  |
| p(C3NDI-T) [7] | Chloroform | 25 | 100-200mgmL | a | This work |
|  | chlorobenzene | 25 | 100-200mgmL | a |  |
|  | o-dichlorobenzene | 25 | 100-200mgmL | a |  |
|  | Toluene | 25 | 100-200mgmL | a |  |
|  | p-xylene | 25 | 100-200mgmL | a |  |
|  | Anisole | 25 | 100-200mgmL | a |  |
| p(C6NDI-T) [7] | Chloroform | 25 | 100-200mgmL | a | This work |
|  | chlorobenzene | 25 | 100-200mgmL | a |  |
|  | o-dichlorobenzene | 25 | 100-200mgmL | a |  |
|  | Toluene | 25 | 100-200mgmL | a |  |
|  | p-xylene | 25 | 100-200mgmL | a |  |
|  | Anisole | 25 | 100-200mgmL | a |  |
| PII [5] | Chlorobenzene | 25 | 10mgmL | i | DOI:10.1021/10.1021/jacs.5c07995 |
|  |  |  | 140mgmL | c |  |
|  |  |  | 170mgmL | c |  |
|  |  |  | 200mgmL | c |  |
| PII-T [5] | Chlorobenzene | 25 | 100mgmL | i | This work |
|  |  |  | 200mgmL | c |  |
|  |  |  | 300mgmL | c |  |
| PII-TT [5] | Chlorobenzene | 25 | 10mgmL | i | DOI:10.1021/10.1021/jacs.5c07995 |
|  |  |  | 100mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 150mgmL | c |  |
|  |  |  | 200mgmL | c |  |
| PTII-2T [5] | Chlorobenzene | 25 | 10mgmL | i | DOI:10.1021/10.1021/jacs.5c07995 |
|  |  |  | 80mgmL | c |  |
|  |  |  | 150mgmL | c |  |
|  |  |  | 200mgmL | c |  |
| PII-3T [5] | Chlorobenzene | 25 | 10-300mgmL | a | DOI:10.1021/10.1021/jacs.5c07995 |
|  | Trichlorobenzene | 25 | 10-200mgmL | a | This work |
|  |  | 190 | 10-200mgmL | a |  |
| PII-TTT [5] | Chlorobenzene | 25 | 100-300mgmL | a | DOI:10.1021/10.1021/jacs.5c07995 |
|  | Chloroform | 25 | 300mgmL | i | This work |
|  | tetrachloroethylene | 25 | 300mgmL | i |  |
| PII-2T (C8-C10) [8] | Chloroform | 25 | 50mgmL | c | This work |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 100mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 200mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  | chlorobenzene | 25 | 50mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 100mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 200mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  | o-dichlorobenzene | 25 | 50mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 100mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 200mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  | Toluene | 25 | 50mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 100mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 200mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  | p-xylene | 25 | 50mgmL | i |  |
|  |  |  |  | i |  |
|  |  |  |  | i |  |
|  |  |  | 100mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 200mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  | Anisole | 25 | 50-200mgmL | i |  |
| PII-2T (C10-C10) - 18.8k [5] | chlorobenzene | 25 | 10mgmL | i | DOI:10.1021/10.1021/jacs.5c07995 |
|  |  |  | 70mgmL | i |  |
|  |  |  | 130mgmL | c |  |
|  |  |  | 200mgmL | c |  |
| PII-2T (C10-C10) - 22.8k [8] | o-dichlorobenzene | 55 | 60mgmL | i | DOI:10.1002/adma.202203055 |
|  |  |  | 130mgmL | c |  |
|  |  |  | 200mgmL | c |  |
|  | Decane | 25 | 60-200mgmL | a |  |
|  |  | 60 | 60-200mgmL | a |  |
|  | Chloronaphthalene | 25 | 60-200mgmL | i |  |
|  |  | 115 | 60-200mgmL | i |  |
| PII-2T (C10-C10) - 23.8k [8] | Chloroform | 25 | 50mgmL | i | This work |
|  |  |  |  | i |  |
|  |  |  |  | i |  |
|  |  |  | 100mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  | chlorobenzene | 25 | 50mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 100mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 200mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  | o-dichlorobenzene | 25 | 50mgmL | i |  |
|  |  |  |  | i |  |
|  |  |  |  | i |  |
|  |  |  | 100mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  | Tetrahydrofuran | 25 | 200mgmL | c |  |
|  | Toluene | 25 | 100-300mgmL | i |  |
|  | p-xylene | 25 | 100-300mgmL | a |  |
|  | Anisole | 25 | 100-300mgmL | a |  |
| DPP2T-T4 [9] | Chlorobenzene | 25 | 60mgmL | i | DOI: 10.1021/acscentsci.3c00775 |
|  |  |  | 100mgmL | c |  |
|  |  |  | 160mgmL | c |  |
|  |  |  | 200mgmL | c |  |
| DPP2T-T2F2 [9] | Chlorobenzene | 25 | 60mgmL | c | DOI: 10.1021/acscentsci.3c00775 |
|  |  |  | 100mgmL | c |  |
|  |  |  | 160mgmL | c |  |
|  |  |  | 200mgmL | c |  |
| DPP-T2M2 [9] | Chlorobenzene | 25 | 60mgmL | i | DOI: 10.1021/acscentsci.3c00775 |
|  |  |  | 100mgmL | i |  |
|  |  |  | 160mgmL | c |  |
|  |  |  | 200mgmL | c |  |
| DPP2T-TT (C4-C10C10) [5] | Chlorobenzene | 25 | 10mgmL | i | DOI:10.1021/10.1021/jacs.5c07995 |
|  |  |  | 100mgmL | c |  |
|  |  |  | 200mgmL | c |  |
|  |  |  | 230mgmL | c |  |
| DPP2T-Btz [5] | Chlorobenzene | 25 | 10mgmL | i | DOI:10.1021/10.1021/jacs.5c07995 |
|  |  |  | 100mgmL | c |  |
|  |  |  | 200mgmL | c |  |
| DPP2T-TT (C2-C8C10) [ossila] | Chloroform | 25 | 50mgmL | c | This work |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 100mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 200mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  | chlorobenzene | 25 | 50mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | i |  |
|  |  |  | 100mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 200mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  | o-dichlorobenzene | 25 | 50mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 100mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 200mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  | Tetrahydrofuran | 25 | 150mgmL | c |  |
|  | Methanesulfonic acid | 25 | 100-300mgmL | a |  |
|  | Toluene | 25 | 50mgmL | i |  |
|  | p-xylene | 25 | 50-100mgmL | a |  |
|  | tetrachloroethylene | 25 | 50mgmL | i |  |
| PyDPP-2T (C8C10) | tetrachloroethylene | 25 | 100mgmL | c | This work |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
| PyDPP-2T (C10C12) | tetrachloroethylene | 25 | 60mgmL | c | This work |
|  |  |  |  | c |  |
|  |  |  | 100mgmL | c |  |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
| PyDPP-2T2F | tetrachloroethylene | 25 | 50mgmL | c | This work |
|  |  |  | 100mgmL | c |  |
|  |  |  |  | c |  |
| PE2-biOE2 [5] | 1,3-dioxane | 25 | 10mgmL | i | DOI:10.1021/10.1021/jacs.5c07995 |
|  |  |  | 90mgmL | c |  |
|  | o-dichlorobenzene | 25 | 200mgmL | c | This work |
|  |  |  |  | c |  |
|  | Anisole | 25 | 200mgmL | c | This work |
| PE2-biOE3 [5] | 1,3-dioxane | 25 | 10mgmL | i | DOI:10.1021/10.1021/jacs.5c07995 |
|  |  |  | 150mgmL | c |  |
| ProDOT(OE3)-co-ProDOT(Oct) | Chloroform | 25 | 100-300mgmL | i | This work |
| ProDOT(OE3)-co-ProDOT(EtHx) [5] | Chloroform | 25 | 10mgmL | i | DOI:10.1021/10.1021/jacs.5c07995 |
|  |  |  | 50mgmL | i |  |
|  |  |  | 100mgmL | c |  |
|  |  |  | 200mgmL | c |  |
| PE2-biOE2OE3 - 16k [5,10] | Chlorobenzene | 25 | 50mgmL | i | This work |
|  |  |  | 100mgmL | c |  |
|  |  |  | 200mgmL | c |  |
|  | 1,3-dioxane | 25 | 200mgmL | c | This work |
|  | 60% chlrobenzene + 40% anisole | 25 | 50mgmL | i | This work |
|  |  |  | 100mgmL | c |  |
|  |  |  | 200mgmL | c |  |
| PE2-biOE2OE3 - 19.8k [5,10] | Chlorobenzene | 25 | 50mgmL | i | This work |
|  |  |  | 100mgmL | c |  |
|  |  |  | 150mgmL | c |  |
| PE2-biOE2OE3 - 20k [5,10] | 1,3-dioxane | 25 | 10mgmL | i | DOI:10.1038/s41467-025-62915-3, DOI:10.1021/10.1021/jacs.5c07995 |
|  |  |  | 60mgmL | i |  |
|  |  |  | 90mgmL | c |  |
|  |  |  | 100mgmL | c |  |
|  |  |  | 120mgmL | c |  |
|  |  |  | 150mgmL | c |  |
|  | diglyme | 25 | 60mgmL | i |  |
|  |  |  | 90mgmL | c |  |
|  |  |  | 120mgmL | c |  |
|  |  |  | 150mgmL | c |  |
|  | 1,4-Dioxane | 25 | 60-150mgmL | i |  |
| PM7 [5] | Chlorobenzene | 25 | 100-300mgmL | a | DOI:10.1021/10.1021/jacs.5c07995 |
| PM7 D1 [5] | Chlorobenzene | 25 | 100-300mgmL | i |  |
| PM7 D2 [5] | Chlorobenzene | 25 | 100-300mgmL | i |  |
| PM7 3ET2 [5] | Chlorobenzene | 25 | 100-300mgmL | i |  |
| PM7 2ET2 [5] | Chlorobenzene | 25 | 100-300mgmL | i |  |
| TPT-E (C8/C10) | Chlorobenzene | 25 | 100-300mgmL | i | This work |
| TPT-2E (C8/C10) | Chlorobenzene | 25 | 100-300mgmL | i | This work |
| T(OE3)P(OC8)-E | chloroform | 25 | 100-300mgmL | i | This work |
| T(OE3)P(OE3)-E | Chloroform | 25 | 100-300mgmL | i | This work |
|  | Anisole | 25 | 100-300mgmL | i |  |
|  |  | 130 | 100-300mgmL | i |  |
|  | o-dichlorobenzene | 25 | 100-300mgmL | i |  |
|  |  | 130 | 100-300mgmL | i |  |
|  | chlorobenzene | 25 | 100-300mgmL | i |  |
|  | Toluene | 25 | 100-300mgmL | i |  |
|  | p-xylene | 25 | 100-300mgmL | i |  |
| TPT-T (C8/C10) | Chlorobenzene | 25 | 100-300mgmL | i | This work |
| BBL - 58.0k [11] | methanesulfonic acid | 25 | 45mgmL | c | This work |
|  | methanesulfonic acid : dipropylamine = 20:1 | 25 | 45mgmL | c |  |
|  | methanesulfonic acid : dipropylamine = 10:1 | 25 | 45mgmL | c |  |
|  | methanesulfonic acid : dipropylamine = 5:1 | 25 | 45mgmL | c |  |
|  | methanesulfonic acid : dipropylamine = 3:1 | 25 | 45mgmL | c |  |
|  | methanesulfonic acid : dipropylamine = 2:1 | 25 | 45mgmL | a |  |
| BBL - 39.3k [11] | methanesulfonic acid | 25 | 45mgmL | c | This work |
| BBL - 102.5k [11] | methanesulfonic acid | 25 | 45mgmL | c | This work |
| BBB - 59.7k [11] | methanesulfonic acid | 25 | 45mgmL | i | This work |
|  |  | 25 | 300mgmL | i |  |
|  | Chloroform | 25 | 300mgmL | a |  |
|  | Chlorobenzene | 25 | 300mgmL | a |  |
| BBB - 40.8k [11] | methanesulfonic acid | 25 | 45mgmL | i | This work |
|  | methanesulfonic acid | 25 | 300mgmL | i |  |
|  | Chloroform | 25 | 300mgmL | a |  |
|  | Chlorobenzene | 25 | 300mgmL | a |  |
| D18 [Ossila] | Chloroform | 25 | 35mgmL | c | This work |
|  |  |  |  | c |  |
|  |  |  |  | c |  |
|  |  |  | 50mgmL | c |  |
|  |  |  | 70mgmL | c |  |
| IDTBT [1-Material] | Chlorobenzene | 25 | 10mgmL | i | DOI:10.1021/10.1021/jacs.5c07995 |
|  |  |  | 150mgmL | c |  |
|  |  |  | 200mgmL | c |  |
| F8BT [Lumtech] | Chlorobenzene | 25 | 150mgmL | c | This work |
|  |  |  | 200mgmL | c |  |
|  |  |  | 250mgmL | c |  |
|  |  |  | 300mgmL | c |  |
|  | Toluene | 25 | 300mgmL | c |  |
|  | Chloroform | 25 | 300mgmL | c |  |

Synthesis Details of TPT-E derivatives

Monomer Synthesis

2,5-dibromo-3,4-ethylenedioxythiophene [dibromo-EDOT]12:

3,4-Ethylenedioxythiophene (3.2 g, 22.7 mmol, 1 eq.), 100 mL of anhydrous THF, and 100 mL of glacial acetic acid were added to a 250 mL round-bottom flask equipped with a magnetic stir bar. The solution was degassed by sparging with argon for 10 minutes, and the reaction vessel was cooled to 0 °C in an ice bath. N-Bromosuccinimide (8.5 g, 47.8 mmol, 2.1 eq.) was added slowly, and the reaction was stirred at room temperature for 4 hours while protected from light. The reaction mixture was then poured into 500 mL of cold distilled water, resulting in a white precipitate that was filtered and washed with distilled water. The filtrate was diluted with an additional 200 mL of distilled water and stored in the refrigerator overnight. The additional precipitate was filtered, combined with the initial solid, and dried under high vacuum overnight to obtain white crystals (6.7 g, 98% yield). 1H NMR (500 MHz, CDCl3) δ 4.29 (s, 4H). 13C NMR (126 MHz, CDCl3) δ 139.71, 85.55, 77.28, 77.23, 77.03, 76.77, 64.98.

Figure S3. 1H NMR spectrum of 2,5-dibromo-3,4-ethylenedixoythiophene [dibromo-EDOT].

Figure S4. 13C NMR spectrum of 2,5-dibromo-3,4-ethylenedixoythiophene [dibromo-EDOT].

2,2’,3,3’-tetrahydro-5,5’-bithieno[3,4-b][1,4]dioxine [Bi-EDOT]13 :

A published protocol was followed with slight modifications. 3,4-Ethylenedioxythiophene (2.85 g, 21 mmol, 1 eq.) and 100 mL of anhydrous THF were added to a 250 mL two-neck Schlenk flask. The vessel was sparged with argon (x3), maintained under an inert atmosphere, and cooled to −78 °C using an acetone/dry ice bath. A 2.5 M solution of n-butyllithium (8.9 mL, 21 mmol, 1 eq.) was added dropwise. After stirring at −78 °C for 30 minutes, CuCl2 (2.7 g, 21 mmol, 1 eq.) was added. The reaction was stirred overnight under argon while warming gradually to room temperature. Methanol (1 mL) was added, and the reaction mixture was concentrated in vacuo and redissolved in dichloromethane. The organic phase was washed with dH2O (x3) and brine (x1). The combined organic fractions were dried over sodium sulfate, filtered, and concentrated in vacuo. The crude product was purified by silica gel chromatography using 100% DCM to obtain a light yellow solid (4.36 g, 73% yield). 1H NMR (500 MHz, CDCl3) δ 6.29 (s, 2H), 4.40–4.30 (m, 4H), 4.29–4.21 (m, 4H). 13C NMR (126 MHz, CDCl3) δ 141.25, 137.05, 109.93, 97.55, 77.27, 77.22, 77.02, 76.76, 65.01, 64.61.

Figure S5. 1H NMR spectrum of 2,2’,3,3’-tetrahydro-5,5’-bithieno[3,4-b][1,4]dioxine [Bi-EDOT].

.

Figure S6. 13C NMR spectrum of 2,2’,3,3’-tetrahydro-5,5’-bithieno[3,4-b][1,4]dioxine [Bi-EDOT].

7,7‘-dibromo-2,2‘,3,3‘-tetrahydro-5,5‘-bithieno[3,4-b][1,4]dioxine [dibromo Bi-EDOT]:

Bi-EDOT (1.1 g, 3.9 mmol, 1 eq.), 6 mL of anhydrous acetonitrile, and 50 mL of anhydrous chloroform were added to a 250 mL round-bottom flask equipped with a magnetic stir bar. The reaction vessel was cooled to −20 °C using a sodium chloride/ice bath mixture (1:3 ratio). N-Bromosuccinimide (1.7 g, 9.8 mmol, 2.5 eq.) was added slowly, and the reaction was stirred at −20 °C for 30 minutes while protected from light. The reaction mixture was immediately poured into 500 mL of ethanol, resulting in a gray-blue precipitate. The solid was filtered and washed with ethanol to obtain a light gray-blue powder (1.2 g, 70% yield). 1H NMR (500 MHz, DMSO) δ 4.65–3.98 (m, 8H). 13C NMR (126 MHz, DMSO) δ 140.27, 136.85, 108.72, 85.34, 65.64, 65.32, 40.49, 40.41, 40.32, 40.25, 40.16, 40.08, 39.99, 39.91, 39.82, 39.73, 39.66, 39.49.

Figure S7. 1H NMR spectrum of 7,7‘-dibromo-2,2‘,3,3‘-tetrahydro-5,5‘-bithieno[3,4-b][1,4]dioxine [dibromo Bi-EDOT].

Figure S8. 13C NMR spectrum of 7,7‘-dibromo-2,2‘,3,3‘-tetrahydro-5,5‘-bithieno[3,4-b][1,4]dioxine [dibromo Bi-EDOT].

7,7‘-bis(trimethylstannyl)2,2‘,3,3‘-tetrahydro-5,5‘-bithieno[3,4-b][1,4]dioxine [Bis-trimethyltin Bi-EDOT]:

Bi-EDOT (1.0 g, 3.5 mmol, 1 eq.) and 50 mL of anhydrous THF were added to a 250 mL two-neck Schlenk flask. The vessel was sparged with argon (x3), maintained under an inert atmosphere, and cooled to −78 °C using an acetone/dry ice bath. A 2.5 M solution of n-butyllithium (2.9 mL, 7.3 mmol, 2.1 eq.) was added dropwise. After the addition was complete, the reaction was stirred at −78 °C for 2 hours, and a 1.0 M trimethyltin solution (7.6 mL, 7.3 mmol, 2.1 eq.) was added. The reaction was stirred overnight while warming gradually to room temperature. The mixture was concentrated under vacuum, redissolved in dichloromethane, and washed with dH2O (x3) and brine (x1). The combined organic fractions were dried over sodium sulfate, filtered, and concentrated in vacuo. The product was washed with hexanes and methanol to obtain a white solid (1.9 g, 88% yield). 1H NMR (500 MHz, CDCl3) δ 4.49–4.11 (m, 8H), 0.38 (s, 18H). 13C NMR (126 MHz, CDCl3) δ 147.36, 137.75, 125.75, 116.05, 106.57, 77.27, 77.22, 77.02, 76.76, 64.96, 64.61, −8.44.

Figure S9. 1H NMR spectrum of 7,7‘-bis(trimethylstannyl)2,2‘,3,3‘-tetrahydro-5,5‘-bithieno[3,4-b][1,4]dioxine [Bis-trimethyltin Bi-EDOT].

Figure S10. 13C NMR spectrum of 7,7‘-bis(trimethylstannyl)2,2‘,3,3‘-tetrahydro-5,5‘-bithieno[3,4-b][1,4]dioxine [Bis-trimethyltin Bi-EDOT].

1,4-bis(octyloxy)benzene14:

Hydroquinone (2.5 g, 22.7 mmol, 1 eq.), anhydrous potassium carbonate (12.5 g, 90.8 mmol, 4 eq.), and 100 mL of anhydrous DMF were added to a 250 mL round-bottom flask. The reaction was stirred at room temperature for 30 minutes before 1-octyl bromide (17.6 g, 22.7 mmol, 4 eq.) was added. The reaction vessel was placed in an oil bath at 80 °C and stirred overnight. The mixture was concentrated in vacuo, and the crude product was recrystallized from methanol to obtain white crystals (5.4 g, 70% yield). 1H NMR (500 MHz, CDCl3) δ 6.84 (s, 4H), 3.92 (t, J = 6.6 Hz, 4H), 1.86–1.69 (m, 4H), 1.46 (t, J = 7.7 Hz, 4H), 1.41–1.22 (m, 18H), 0.99–0.86 (m, 6H). 13C NMR (126 MHz, CDCl3) δ 153.22, 115.41, 77.27, 77.22, 77.02, 76.76, 68.69, 31.83, 29.42, 29.39, 29.26, 26.08, 22.67, 14.10.

Figure S11. 1H NMR spectrum of 1,4-bis(octyloxy)benzene.

Figure S12. 13C NMR spectrum of 1,4-bis(octyloxy)benzene.

1,4-dibromo-2,5-bis(octyloxy)benzene14 :

1,4-Bis(octyloxy)benzene (2.5 g, 7.5 mmol, 1 eq.) and 100 mL of anhydrous dichloromethane were added to a 250 mL round-bottom flask. The reaction vessel was cooled to 0 °C in an ice bath, and bromine (2.9 g, 17.9 mmol, 2.4 eq.) was added gradually. The reaction was stirred overnight while protected from light and allowed to warm gradually to room temperature. Excess bromine was quenched with Na2S2O3, and the organic phase was washed with dH2O (x3) and brine (x1). The combined organic fractions were dried over sodium sulfate, filtered, and concentrated in vacuo. The crude product was purified by silica gel chromatography using hexanes to obtain white crystals (3.4 g, 70% yield). 1H NMR (400 MHz, CDCl3) δ 7.11 (s, 2H), 3.97 (t, J = 6.5 Hz, 4H), 1.82 (dq, J = 7.9, 6.6 Hz, 4H), 1.50 (qd, J = 6.6, 3.9 Hz, 4H), 1.41–1.27 (m, 16H), 0.97–0.86 (m, 6H). 13C NMR (101 MHz, CDCl3) δ 150.11, 118.52, 111.17, 77.34, 77.02, 76.71, 70.35, 31.81, 29.27, 29.22, 29.14, 25.95, 22.67, 14.11.

Figure S13. 1H NMR spectrum of 1,4-dibromo-2,5-bis(octyloxy)benzene.

Figure S14. 13C NMR spectrum of 1,4-dibromo-2,5-bis(octyloxy)benzene.

Triethylene glycol monomethyl ether tosylate15 :

Potassium hydroxide (6.7 g, 120.1 mmol, 1.4 eq.), triethylene glycol monomethyl ether (13.4 g, 84 mmol, 1 eq.), 25 mL of dH2O, and 25 mL of THF were added to a 250 mL round-bottom flask equipped with a magnetic stir bar. The mixture was stirred for 10 minutes and then cooled to 0 °C in an ice bath. A solution of p-toluenesulfonyl chloride (16.0 g, 84 mmol, 1 eq.) in 25 mL of THF was added dropwise. The reaction was maintained at 0 °C for 2 hours and then stirred overnight at room temperature. The aqueous phase was extracted with diethyl ether (x3), and the combined organic fractions were washed with dH2O (x3) and brine (x1), dried over sodium sulfate, filtered, and concentrated in vacuo to obtain a clear oil (19.9 g, 71% yield). 1H NMR (500 MHz, CDCl3) δ 7.94–7.71 (m, 2H), 7.35 (d, J = 8.0 Hz, 2H), 4.37–4.08 (m, 2H), 3.77–3.65 (m, 2H), 3.65–3.55 (m, 6H), 3.55–3.45 (m, 2H), 3.38 (s, 3H), 2.45 (s, 3H). 13C NMR (126 MHz, CDCl3) δ 144.79, 133.04, 129.82, 127.98, 77.32, 77.27, 77.07, 76.81, 71.91, 70.74, 70.56, 70.54, 69.24, 68.67, 59.02, 21.63.

Figure S15. 1H NMR spectrum of triethylene glycol monomethyl ether tosylate.

Figure S16. 13C NMR spectrum of triethylene glycol monomethyl ether tosylate.

1,4-dibromo-2,5-bis(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)benzene16 :

2,5-Dibromohydroquinone (1.5 g, 5.6 mmol, 1 eq.) and 25 mL of anhydrous THF were added to a 250 mL round-bottom flask equipped with a magnetic stir bar under an argon atmosphere. A solution of potassium hydroxide (0.64 g, 11.4 mmol, 2 eq.) in 20 mL of ethanol was added slowly, and the reaction was stirred at room temperature for 3 hours. Triethylene glycol monomethyl ether tosylate (3.64 g, 11.4 mmol, 2 eq.) dissolved in 25 mL of anhydrous THF was then added. The reaction vessel was heated to 50 °C and stirred overnight. The reaction mixture was concentrated in vacuo, redissolved in diethyl ether, and washed with brine (x1). The combined organic fractions were dried over sodium sulfate, filtered, and concentrated in vacuo. The crude product was purified by silica gel chromatography using a gradient of 1:1 hexanes/ethyl acetate to 100% ethyl acetate to obtain a pale-yellow oil (1.7 g, 53% yield). 1H NMR (500 MHz, CDCl3) δ 7.17 (s, 2H), 4.14 (t, J = 4.8 Hz, 4H), 3.89 (t, J = 4.8 Hz, 4H), 3.78 (dd, J = 5.8, 3.8 Hz, 4H), 3.69 (ddd, J = 9.3, 5.3, 3.2 Hz, 8H), 3.57 (dd, J = 5.9, 3.5 Hz, 4H), 3.39 (s, 6H). 13C NMR (126 MHz, CDCl3) δ 150.34, 119.18, 111.39, 77.29, 77.24, 77.04, 76.79, 71.97, 71.10, 70.74, 70.60, 70.21, 69.59, 59.05.

Figure S17. 1H NMR spectrum of 1,4-dibromo-2,5-bis(2-(2-(2 methoxyethoxy)ethoxy)ethoxy) benzene.

Figure S18. 13C NMR spectrum of 1,4-dibromo-2,5-bis(2-(2-(2 methoxyethoxy)ethoxy)ethoxy) benzene.

3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophene17 :

3-Methoxythiophene (4.0 g, 35.0 mmol, 1 eq.), triethylene glycol monomethyl ether (8.6 g, 53 mmol, 1.50 eq.), p-toluenesulfonic acid (0.62 g, 3.5 mmol, 0.1 eq.), and 150 mL of anhydrous toluene were added to a 250 mL three-neck round-bottom flask equipped with a magnetic stir bar and reflux condenser under an argon atmosphere. The flask was purged with argon, and the reaction was refluxed overnight. During reflux, the vessel was briefly placed under vacuum once per hour to remove methanol byproduct and then refilled with argon. The reaction mixture was concentrated to dryness, and the crude product was purified by silica gel chromatography using a gradient of 4:1 hexanes/DCM to obtain a pale-yellow viscous oil (4.5 g, 52% yield). 1H NMR (500 MHz, CDCl3) δ 7.17 (dd, J = 5.2, 3.1 Hz, 1H), 6.78 (dd, J = 5.2, 1.6 Hz, 1H), 6.27 (dd, J = 3.2, 1.6 Hz, 1H), 4.18–4.06 (m, 2H), 3.93–3.80 (m, 2H), 3.78–3.71 (m, 2H), 3.71–3.60 (m, 4H), 3.60–3.49 (m, 2H), 3.39 (s, 3H). 13C NMR (126 MHz, CDCl3) δ 157.61, 124.64, 119.60, 97.51, 77.35, 77.10, 76.84, 71.94, 70.79, 70.66, 70.58, 69.70, 69.58, 59.04.

Figure S19. 1H NMR spectrum of 3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophene.

Figure S20. 13C NMR spectrum of 3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophene.

Triisopropyl(3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophen-2-yl)silane18:

3-(2-(2-(2-Methoxyethoxy)ethoxy)ethoxy)thiophene (6.2 g, 25.1 mmol, 1 eq.) and 100 mL of anhydrous THF were added to a 250 mL Schlenk flask equipped with a magnetic stir bar under an argon atmosphere. The solution was cooled to −78 °C using a dry ice/acetone bath, and a 2.5 M solution of n-butyllithium (10.6 mL, 26.5 mmol, 1.1 eq.) was added dropwise. After the addition was complete, the reaction was stirred at −78 °C for 1 hour, and triisopropylsilyl chloride (5.6 g, 28.9 mmol, 1.2 eq.) was added slowly. The reaction was stirred overnight while warming gradually to room temperature. The reaction mixture was concentrated to dryness, redissolved in diethyl ether, and washed with dH2O (x3) and brine (x1). The combined organic fractions were dried over sodium sulfate, filtered, and concentrated under vacuum. The crude product was purified by silica gel chromatography using a gradient of 100% hexanes to 30% ethyl acetate in hexanes to obtain a clear oil (9.5 g, 95% yield). 1H NMR (300 MHz, CDCl3) δ 7.44 (d, J = 5.0 Hz, 1H), 6.92 (d, J = 5.0 Hz, 1H), 4.11 (dd, J = 6.7, 3.6 Hz, 2H), 3.77 (t, J = 5.2 Hz, 2H), 3.73–3.58 (m, 8H), 3.57–3.51 (m, 2H), 3.37 (s, 3H), 1.42–1.33 (m, 3H), 1.08 (dd, J = 7.3, 2.6 Hz, 18H). 13C NMR (75 MHz, CDCl3) δ 163.59, 129.83, 116.48, 108.95, 77.46, 77.04, 76.62, 71.92, 70.69, 70.64, 70.58, 70.03, 69.93, 59.04, 18.81, 18.76, 18.61, 18.52, 17.70, 12.04, 12.00.

Figure S21. 1H NMR spectrum of Triisopropyl(3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy) thiophen-2-yl)silane.

Figure S22. 13C NMR spectrum of Triisopropyl(3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy) thiophen-2-yl)silane.

2-(4-decylthiophen-2-yl)-4,4,5,5-tetramethyl-1,3,2-dioxaborolane19 :

3-Decylthiophene (1.1 g, 4.9 mmol, 1 eq.) and 100 mL of anhydrous THF were added to a 250 mL two-neck round-bottom Schlenk flask under an argon atmosphere. The reaction vessel was cooled to 0 °C in an ice bath, and a 2.0 M solution of LDA (3.0 mL, 6.0 mmol, 1 eq.) was added dropwise. After the addition was complete, the reaction was stirred at 0 °C for 1 hour. The temperature was then lowered to −78 °C using an acetone/dry ice bath, and 2-isopropoxy-4,4,5,5-tetramethyl-1,3,2-dioxaborolane (1.2 g, 6.6 mmol, 1.1 eq.) was added carefully. The reaction was stirred overnight while warming gradually to room temperature. The mixture was concentrated under vacuum, redissolved in diethyl ether, and washed with dH2O (x3) and brine (x1). The combined organic fractions were dried over sodium sulfate, filtered, and concentrated under vacuum. The crude product was purified by silica gel chromatography using a gradient of 100% hexanes to 10% DCM in hexanes to obtain a clear oil (0.68 g, 40% yield). 1H NMR (500 MHz, CDCl3) δ 7.50 (d, J = 1.2 Hz, 1H), 7.24 (t, J = 1.0 Hz, 1H), 2.72–2.54 (m, 2H), 1.64 (d, J = 2.9 Hz, 2H), 1.37 (s, 12H), 1.34 (d, J = 16.2 Hz, 6H), 1.29 (s, 10H), 0.91 (t, J = 6.9 Hz, 3H). 13C NMR (126 MHz, CDCl3) δ 144.73, 138.51, 127.57, 84.00, 77.30, 77.04, 76.79, 31.95, 31.93, 30.68, 30.00, 29.68, 29.66, 29.64, 29.60, 29.48, 29.38, 29.36, 29.33, 24.80, 24.78, 22.71, 14.14.

Figure S23. 1H NMR spectrum of 2-(4-decylthiophen-2-yl)-4,4,5,5-tetramethyl-1,3,2-dioxaborolane.

Figure S24. 13C NMR spectrum of 2-(4-decylthiophen-2-yl)-4,4,5,5-tetramethyl-1,3,2-dioxaborolane.

5,5’-(2,5’bis(octyloxy)-1,4-phenylene)bis(3-decylthiophene) (TPT C10/C8)20 :

2-(4-Decylthiophen-2-yl)-4,4,5,5-tetramethyl-1,3,2-dioxaborolane (0.5 g, 1.4 mmol, 2.5 eq.), dry potassium carbonate (0.24 g, 1.7 mmol, 3 eq.), 1,4-dibromo-2,5-bis(octyloxy)benzene (0.28 mg, 0.6 mmol, 1 eq.), Pd(dppf)Cl2·DCM (0.050 g, 0.06 mmol, 0.1 eq.), and 20 mL of anhydrous DMF were added to a 100 mL round-bottom flask equipped with a magnetic stir bar in a glovebox. The reaction vessel was capped in the glovebox, removed, and placed in an oil bath at 110 °C overnight. The mixture was then concentrated under vacuum, and the crude product was purified by silica gel chromatography using a gradient of 100% hexanes to 10% DCM in hexanes to obtain a yellow oil that solidified upon standing (0.36 g, 81% yield). 1H NMR (500 MHz, CDCl3) δ 7.40 (d, J = 1.4 Hz, 2H), 7.22 (s, 2H), 6.94 (d, J = 1.4 Hz, 2H), 4.09 (t, J = 6.5 Hz, 4H), 2.65 (t, J = 7.8 Hz, 4H), 1.96–1.86 (m, 4H), 1.68 (t, J = 7.8 Hz, 4H), 1.57–1.50 (m, 4H), 1.42–1.24 (m, 50H), 0.91 (td, J = 6.9, 4.7 Hz, 12H). 13C NMR (126 MHz, CDCl3) δ 149.31, 143.02, 138.97, 126.80, 123.01, 120.36, 112.73, 77.28, 77.23, 77.03, 76.78, 69.69, 31.94, 31.87, 30.66, 30.60, 29.67, 29.64, 29.56, 29.50, 29.45, 29.43, 29.37, 29.36, 29.30, 26.34, 22.71, 14.14.

Figure S25. 1H NMR spectrum of 5,5’-(2,5’bis(octyloxy)-1,4-phenylene)bis(3-decylthiophene) (TPT C10/C8).

Figure S26. 13C NMR spectrum of 5,5’-(2,5’bis(octyloxy)-1,4-phenylene)bis(3-decylthiophene) (TPT C10/C8).

5,5’-(2,5’bis(octyloxy)-1,4-phenylene)bis(2-bromo3-decylthiophene) (dibromo TPT C10/C8)20 :

TPT C10/C8 monomer (0.57 g, 0.73 mmol, 1 eq.), N-bromosuccinimide (0.26 g, 1.5 mmol, 2.1 eq.), and 100 mL of dichloromethane were added to a 100 mL round-bottom flask equipped with a magnetic stir bar. The reaction vessel was covered with aluminum foil and stirred overnight at room temperature. The mixture was then washed with dH2O (x3) and brine (x1). The combined organic fractions were dried over sodium sulfate, filtered, and concentrated under vacuum. The crude product was purified by silica gel chromatography using a gradient of 100% hexanes to 5% DCM in hexanes to obtain a bright yellow powder (0.62 g, 90% yield). 1H NMR (500 MHz, CDCl3) δ 7.22 (s, 2H), 7.15 (s, 2H), 4.10 (t, J = 6.5 Hz, 4H), 2.60 (t, J = 7.7 Hz, 4H), 1.93 (p, J = 6.7 Hz, 4H), 1.68–1.59 (m, 4H), 1.55 (d, J = 7.1 Hz, 6H), 1.45–1.23 (m, 45H), 0.91 (q, J = 7.1 Hz, 12H). 13C NMR (126 MHz, CDCl3) δ 149.17, 141.53, 138.31, 125.55, 122.52, 111.47, 110.04, 77.27, 77.22, 77.02, 76.76, 69.83, 31.92, 31.85, 29.88, 29.65, 29.63, 29.49, 29.41, 29.39, 29.36, 29.34, 29.27, 26.31, 22.69, 14.12.

Figure S27. 1H NMR spectrum of 5,5’-(2,5’bis(octyloxy)-1,4-phenylene)bis(2-bromo3-decylthiophene) (dibromo TPT C10/C8).

Figure S28. 13C NMR spectrum of 5,5’-(2,5’bis(octyloxy)-1,4-phenylene)bis(2-bromo3-decylthiophene) (dibromo TPT C10/C8).

((2,5-bis(octyloxy)-1,4-phenylene)bis(3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophene-5,2-diyl))bis(triisopropylsilane) TIPS-(T(OE3)P(OC8)18 :

Triisopropyl(3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophen-2-yl)silane (1.5 g, 3.7 mmol, 2.2 eq.), 1,4-dibromo-2,5-bis(octyloxy)benzene (0.83 g, 1.7 mmol, 1 eq.), cesium carbonate (1.8 g, 5.6 mmol, 3.3 eq.), palladium(II) acetate (0.015 g, 0.07 mmol, 0.04 eq.), cesium pivalate (0.87 g, 3.7 mmol, 2.2 eq.), tris(2-methoxyphenyl)phosphine (0.054 mg, 0.15 mmol, 0.1 eq.), and 10 mL of anhydrous toluene were added to a 100 mL round-bottom flask equipped with a magnetic stir bar in a glovebox. The reaction vessel was capped in the glovebox, removed, and placed on a hot plate at 110 °C for 72 hours while protected from light. The reaction mixture was concentrated in vacuo, and the crude product was purified by silica gel chromatography using a gradient of 1:1 hexanes/EtOAc to 100% EtOAc to obtain a red oil (1.8 g, 95% yield). 1H NMR (500 MHz, CDCl3) δ 7.43 (s, 2H), 7.21 (s, 2H), 4.21 (t, J = 5.2 Hz, 4H), 4.11 (t, J = 6.3 Hz, 4H), 3.83 (t, J = 5.2 Hz, 4H), 3.77–3.71 (m, 4H), 3.71–3.66 (m, 8H), 3.58 (t, J = 4.7 Hz, 4H), 3.40 (s, 6H), 1.93 (dd, J = 8.8, 6.2 Hz, 4H), 1.62–1.55 (m, 4H), 1.45 (d, J = 7.5 Hz, 3H), 1.31 (s, 4H), 1.18–1.11 (m, 36H), 1.08 (s, 6H), 0.90 (d, J = 7.2 Hz, 6H). 13C NMR (126 MHz, CDCl3) δ 162.93, 149.49, 143.09, 122.82, 114.65, 111.84, 109.92, 77.27, 77.22, 77.02, 76.77, 71.97, 70.74, 70.62, 70.07, 69.87, 69.71, 59.05, 31.92, 29.68, 29.61, 29.36, 26.62, 22.70, 18.86, 18.83, 18.78, 18.64, 17.71, 14.12, 12.30, 12.13, 12.07, 12.04.

Figure S29. 1H NMR spectrum of ((2,5-bis(octyloxy)-1,4-phenylene)bis(3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophene-5,2-diyl))bis(triisopropylsilane) TIPS-(T(OE3)P(OC8).

Figure S30. 13C NMR spectrum of ((2,5-bis(octyloxy)-1,4-phenylene)bis(3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophene-5,2-diyl))bis(triisopropylsilane) TIPS-(T(OE3)P(OC8).

5,5’-(2,5-bis(octyloxy)-1,4-phenylene)bis(3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophene) [H-T(OE3)P(OC8)-H]18 :

TIPS-protected T(OE3)P(OC8) monomer (1.1 g, 1.0 mmol, 1 eq.) and 25 mL of anhydrous THF were added to a 100 mL round-bottom flask equipped with a stir bar under an inert atmosphere. A 1.0 M solution of TBAF in THF (2.0 mL, 2 mmol, 2.1 eq.) was added, and the reaction was stirred overnight at room temperature. The reaction mixture was concentrated in vacuo, redissolved in diethyl ether, and washed with brine (x1). The combined organic fractions were dried over sodium sulfate, filtered, and concentrated under vacuum. The crude product was purified by silica gel chromatography using a gradient of 1:1 hexanes/EtOAc to 100% EtOAc to obtain a yellow oil (0.56 g, 70% yield). 1H NMR (500 MHz, CDCl3) δ 7.39 (s, 2H), 7.26 (s, 2H), 6.93 (s, 2H), 4.26 (t, J = 5.1 Hz, 4H), 3.97 (t, J = 5.1 Hz, 4H), 3.78 (dd, J = 5.7, 3.9 Hz, 4H), 3.71 (dd, J = 6.0, 3.7 Hz, 4H), 3.67 (dd, J = 5.7, 3.8 Hz, 4H), 3.56 (t, J = 4.7 Hz, 4H), 3.39 (s, 6H), 2.64 (t, J = 7.7 Hz, 4H), 1.74–1.63 (m, 4H), 1.40–1.27 (m, 28H), 0.90 (t, J = 6.8 Hz, 6H). 13C NMR (126 MHz, CDCl3) δ 149.35, 143.07, 138.64, 126.98, 123.42, 120.54, 113.43, 77.28, 77.23, 77.03, 76.77, 71.96, 70.89, 70.73, 70.61, 69.84, 69.12, 59.04, 31.93, 30.65, 30.60, 29.67, 29.55, 29.45, 29.36, 22.70, 14.13.

Figure S31. 1H NMR spectrum of 5,5’-(2,5-bis(octyloxy)-1,4-phenylene)bis(3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophene) [H-T(OE3)P(OC8)-H].

Figure S32. 13C NMR spectrum of 5,5’-(2,5-bis(octyloxy)-1,4-phenylene)bis(3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophene) [H-T(OE3)P(OC8)-H].

Synthesis of ((2,5-bis(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)-1,4-phenylene)bis(3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophene-5,2-diyl))bis(triisopropylsilane) TIPS-T(OE3)P(OE3)18 :

Triisopropyl(3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophen-2-yl)silane (1.5 g, 3.7 mmol, 2.2 eq.), 1,4-dibromo-2,5-bis(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)benzene (0.95 g, 1.7 mmol, 1 eq.), cesium carbonate (1.8 g, 5.6 mmol, 3.3 eq.), palladium(II) acetate (0.015 g, 0.07 mmol, 0.04 eq.), cesium pivalate (0.87 g, 3.7 mmol, 2.2 eq.), tris(2-methoxyphenyl)phosphine (0.054 mg, 0.15 mmol, 0.1 eq.), and 10 mL of anhydrous toluene were added to a 100 mL round-bottom flask equipped with a magnetic stir bar in a glovebox. The reaction vessel was capped in the glovebox, removed, and placed on a hot plate at 110 °C for 72 hours while protected from light. The reaction mixture was concentrated in vacuo, and the crude product was purified by silica gel chromatography using a gradient of 1:1 hexanes/EtOAc to 100% EtOAc and then 10% MeOH in DCM to obtain a red oil (1.9 g, 89% yield). 1H NMR (500 MHz, CDCl3) δ 7.49 (s, 2H), 7.23 (s, 2H), 4.28 (t, J = 5.1 Hz, 4H), 4.20 (t, J = 5.2 Hz, 4H), 3.97 (t, J = 5.1 Hz, 4H), 3.83 (t, J = 5.2 Hz, 4H), 3.76 (dd, J = 5.8, 3.8 Hz, 4H), 3.74–3.71 (m, 4H), 3.68 (td, J = 5.5, 3.0 Hz, 12H), 3.66–3.62 (m, 4H), 3.58 (d, J = 4.9 Hz, 4H), 3.55 (dd, J = 5.7, 3.9 Hz, 4H), 3.40 (s, 6H), 3.38 (d, J = 3.3 Hz, 6H), 1.45 (q, J = 7.4 Hz, 6H), 1.14 (d, J = 7.3 Hz, 36H). 13C NMR (126 MHz, CDCl3) δ 163.14, 149.42, 142.82, 123.24, 115.37, 112.68, 109.73, 77.27, 77.22, 77.02, 76.77, 71.97, 71.93, 70.84, 70.73, 70.71, 70.62, 70.58, 70.07, 69.90, 69.82, 68.95, 59.05, 59.02, 53.42, 18.88, 18.65, 12.13.

Figure S33. 1H NMR spectrum of ((2,5-bis(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)-1,4-phenylene)bis(3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophene-5,2-diyl))bis(triisopropylsilane) TIPS-T(OE3)P(OE3).

Figure S34. 13C NMR spectrum of ((2,5-bis(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)-1,4-phenylene)bis(3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophene-5,2-diyl))bis(triisopropylsilane) TIPS-T(OE3)P(OE3).

5,5’-(2,5-bis(2-(2-(2-(methoxyethoxy)ethoxy)ethoxy)-1,4-phenylene)bis(3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophene) [H-T(OE3)P(OE3)-H]18 :

TIPS-protected T(OE3)P(OE3) monomer (1.1 g, 1.0 mmol, 1 eq.) and 25 mL of anhydrous THF were added to a 100 mL round-bottom flask equipped with a stir bar under an inert atmosphere. A 1.0 M solution of TBAF in THF (1.9 mL, 2 mmol, 2.1 eq.) was added, and the reaction was stirred overnight at room temperature. The reaction mixture was concentrated in vacuo, redissolved in diethyl ether, and washed with brine (x1). The combined organic fractions were dried over sodium sulfate, filtered, and concentrated under vacuum. The crude product was purified by silica gel chromatography using a gradient of 100% DCM to 10% MeOH in DCM to obtain a yellow oil (0.67 g, 65% yield). 1H NMR (500 MHz, CDCl3) δ 7.27 (d, J = 1.6 Hz, 2H), 7.22 (s, 2H), 6.29 (d, J = 1.7 Hz, 2H), 4.24 (t, J = 5.1 Hz, 4H), 4.17 (t, J = 4.9 Hz, 4H), 3.96 (t, J = 5.1 Hz, 4H), 3.88 (t, J = 4.9 Hz, 4H), 3.79–3.75 (m, 9H), 3.72 (t, J = 4.8 Hz, 8H), 3.69–3.66 (m, 8H), 3.57 (dd, J = 7.8, 4.7 Hz, 8H), 3.41 (s, 6H), 3.39 (s, 6H). 13C NMR (126 MHz, CDCl3) δ 156.91, 149.56, 137.57, 123.26, 117.89, 112.99, 98.34, 77.27, 77.22, 77.02, 76.76, 71.96, 70.90, 70.82, 70.72, 70.70, 70.61, 70.60, 69.78, 69.74, 69.33, 69.10, 59.06, 59.04.

Figure S35. 13C NMR spectrum of 5,5’-(2,5-bis(2-(2-(2-(methoxyethoxy)ethoxy)ethoxy)-1,4-phenylene)bis(3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophene) [H-T(OE3)P(OE3)-H].

Figure S36. 13C NMR spectrum of 5,5’-(2,5-bis(2-(2-(2-(methoxyethoxy)ethoxy)ethoxy)-1,4-phenylene)bis(3-(2-(2-(2-methoxyethoxy)ethoxy)ethoxy)thiophene) [H-T(OE3)P(OE3)-H].

General Polymer Synthesis using Stille Coupling:

Bis trimethyltin EDOT or bis trimethyltin Bi-EDOT (1 eq.) and dibromo TPT monomer (1 eq.) were added to a dry 50 mL round-bottom flask equipped with a stir bar. The flask was transferred to an argon-filled glove box where the catalyst tris(dibenzylideneacetone)dipalladium (0.02 eq), the ligand tris(o-tolyl)phosphine (0.08 eq.), and 4.5 mL of dry toluene were added. The reaction vessel was sealed in the glovebox and removed. The vessel was then placed in an oil bath and the temperature was set to 95 °C, and the mixture was allowed to stir for 72 hours. Afterwards, the temperature was cooled to room temperature, and the product was precipitated by adding to cold methanol. Further purification of crude polymer was achieved through Soxhlet washing with methanol (24 hrs), acetone (24 hrs), and hexanes (24 hrs). The purified polymer was obtained via Soxhlet extraction using chloroform, concentrated in vacuo and reprecipitated into cold methanol to obtain polymer.

TPT-E (C8/10): Shiny dark magenta film (0.42 g, 56% yield). 1H NMR (500 MHz, CD2Cl2) δ 7.51 (s, 2H), 7.29 (s, 2H), 4.40 (s, 4H), 4.18 (t, J = 6.6 Hz, 4H), 2.84 (t, J = 8.0 Hz, 4H), 2.14 – 1.88 (m, 4H), 1.76 (t, J = 7.8 Hz, 4H), 1.63 (q, J = 7.5 Hz, 4H), 1.50 – 1.39 (m, 14H), 1.41 – 1.31 (m, 32H), 0.91 (td, J = 6.8, 4.3 Hz, 15H). 13C NMR (126 MHz, CD2Cl2) δ 149.48, 140.71, 137.92, 127.96, 127.37, 122.67, 112.10, 109.79, 69.79, 64.80, 53.84, 53.62, 53.41, 53.37, 53.19, 52.97, 37.06, 32.73, 31.95, 31.91, 30.78, 30.01, 29.78, 29.74, 29.71, 29.68, 29.65, 29.61, 29.53, 29.48, 29.40, 29.34, 29.29, 27.05, 26.38, 22.70, 19.47, 13.88, 0.75. The number-average molecular weight was 27.6 kg/mol and the dispersity (Đ) was 1.6 with a monomodal distribution as measured by GPC.

Figure S37. 1H NMR spectrum of TPT-E (C8/C10).

Figure S38. 13C NMR spectrum of TPT-E (C8/C10).

Figure S39. Size exclusion chromatogram of TPT-E (C8/C10) in 40 °C CHCl3 (calibrated versus polystyrene standards). The number average molecular weight was determined to be 27.6 kg/mol with a Ð of 1.6

TPT-2E (C8/C10): Shiny black film (0.60 g, 72% yield). 1H NMR (500 MHz, CD2Cl2) δ 7.50 (s, 2H), 7.28 (s, 2H), 4.48 – 4.36 (m, 8H), 4.17 (t, J = 6.4 Hz, 4H), 2.80 (d, J = 8.1 Hz, 4H), 2.02 – 1.95 (m, 4H), 1.73 (d, J = 7.9 Hz, 4H), 1.66 – 1.61 (m, 4H), 1.50 – 1.43 (m, 8H), 1.43 – 1.38 (m, 8H), 1.37 – 1.31 (m, 32H), 0.92 (dt, J = 7.1, 3.4 Hz, 12H). 13C NMR (126 MHz, CD2Cl2) δ 149.47, 140.77, 137.99, 137.66, 137.01, 128.08, 127.60, 122.65, 112.11, 109.12, 108.77, 69.79, 65.04, 64.89, 53.84, 53.63, 53.41, 53.19, 52.98, 31.94, 31.91, 30.69, 29.73, 29.71, 29.69, 29.54, 29.48, 29.45, 29.38, 29.33, 26.38, 22.69, 13.88, 0.75. The number-average molecular weight was 16.5 kg/mol and the dispersity (Đ) was 1.9 with a monomodal distribution as measured by GPC.

Figure S40. 1H NMR spectrum of TPT-2E (C8/C10).

Figure S41. 13C NMR spectrum of TPT-2E (C8/C10).

Figure S42. Size exclusion chromatogram of TPT-2E (C8/C10) in 40 °C CHCl3 (calibrated versus polystyrene standards). The number average molecular weight was determined to be 16.5 kg/mol with a Ð of 1.9.

General Polymer Synthesis Using DHAP Coupling:

Dibromo EDOT or dibromo Bi-EDOT (1 eq.) and the TPT monomer (1 eq.) were added to a dry 50 mL round-bottom flask equipped with a stir bar. The flask was transferred to an argon-filled glovebox, where palladium(II) acetate (0.04 eq.), pivalic acid (0.4 eq.), dry potassium carbonate (2.5 eq.), and 10 mL of dry DMAc were added. The reaction vessel was capped in the glovebox, removed, and placed in an oil bath. The temperature was ramped from 30 °C to 110 °C at 5 °C/min, and the reaction was stirred for 72 hours. After cooling to room temperature, the polymer was precipitated into cold methanol. The crude polymer was further purified by Soxhlet washing with methanol, acetone, and hexanes for 24 hours each. The purified polymer was then extracted with chloroform, concentrated in vacuo, and reprecipitated into cold methanol.

T(OE3)P(OC8)-E: Dark blue/purple powder (0.43 g, 57% yield). 1H NMR (500 MHz, CD2Cl2) δ 7.50 (s, 2H), 7.29 (s, 2H), 4.48 (s, 4H), 4.40 (d, J = 5.6 Hz, 4H), 4.20 (d, J = 6.4 Hz, 4H), 4.01 (t, J = 5.4 Hz, 4H), 3.83 – 3.76 (m, 4H), 3.67 (q, J = 4.3 Hz, 4H), 3.63 – 3.60 (m, 4H), 3.51 (t, J = 4.7 Hz, 4H), 3.34 (s, 6H), 2.03 (q, J = 7.2 Hz, 4H), 1.63 (s, 4H), 1.47 (d, J = 7.7 Hz, 4H), 1.42 (d, J = 7.5 Hz, 4H), 1.36 (d, J = 3.5 Hz, 12H), 0.94 (s, 6H). 13C NMR (126 MHz, CD2Cl2) δ 112.09, 71.91, 71.50, 70.89, 70.85, 70.57, 70.55, 70.46, 70.42, 69.96, 69.81, 69.34, 65.19, 58.59, 58.57, 53.85, 53.63, 53.42, 53.20, 52.99, 37.06, 31.92, 29.68, 27.05, 22.69, 13.87. The number-average molecular weight was 22.0 kg/mol and the dispersity (Đ) was 1.4 with a monomodal distribution measured by GPC.

Figure S43. 1H NMR spectrum of T(OE3)P(OC8)-E.

Figure S44. 13C NMR spectrum of T(OE3)P(OC8)-E.

Figure S45. Size exclusion chromatogram of T(OE3)P(OC8)-E in 40 °C CHCl3 (calibrated versus polystyrene standards). The number average molecular weight was determined to be 22 kg/mol with a Ð of 1.4.

T(OE3)P(OE3)-E: Dark blue/black powder (0.34 g, 62% yield). 1H NMR (500 MHz, CD2Cl2) δ 7.55 (s, 2H), 7.32 (s, 2H), 4.50 (s, 4H), 4.45 – 4.38 (m, 4H), 4.36 (t, J = 5.1 Hz, 4H), 4.05 (q, J = 5.3 Hz, 4H), 4.01 (t, J = 5.1 Hz, 4H), 3.80 (ddd, J = 12.4, 5.8, 3.8 Hz, 8H), 3.69 (ddd, J = 13.8, 6.0, 3.7 Hz, 8H), 3.63 (ddd, J = 8.7, 5.8, 3.7 Hz, 8H), 3.52 (ddd, J = 8.0, 5.9, 3.7 Hz, 8H), 3.35 (d, J = 2.2 Hz, 6H), 3.34 (s, 6H). 13C NMR (126 MHz, CD2Cl2) δ 112.09, 71.91, 71.50, 70.89, 70.85, 70.57, 70.55, 70.46, 70.42, 69.96, 69.81, 69.34, 65.19, 58.59, 58.57, 53.85, 53.63, 53.42, 53.20, 52.99, 37.06, 31.92, 29.68, 27.05, 22.69, 13.87. The number-average molecular weight was 39.0 kg/mol and the dispersity (Đ) was 1.6 with a monomodal distribution measured by GPC.

Figure S46. 1H NMR spectrum of T(OE3)P(OE3)-E.

Figure S47. 13C NMR spectrum of T(OE3)P(OE3)-E.

Figure S48. Size exclusion chromatogram of T(OE3)P(OE3)-E in 40 °C CHCl3 (calibrated versus polystyrene standards). The number average molecular weight was determined to be 39 kg/mol with a Ð of 1.6.

Synthesis Details of ProDOT(OE3)-co-ProDOT(Oct)

ProDOT(OE3)-co-ProDOT(Oct) was synthesized via direct (hetero)arylation polymerization. Briefly, a vessel of pre-dried DMAc, sitting over activated 4 Å molecular sieves, was purged with argon for 2 hours before the polymerization. Then, dihydro-ProDOT(OE3)21 (438 mg, 0.86 mmol), dibromo-octyloxy-ProDOT22 (515 mg, 0.86 mmol), Pd(OAc)2 (4 mg, 0.018 mmol), 0.3 equivalents of pivalic acid (26 mg, 0.254 mmol), and 2.5 equivalents of potassium carbonate (300 mg, 2.17 mmol) were added to a dry 100 mL round bottom flask was equipped with a magnetic stir bar. The round bottom was then transferred into a glove box where it was sealed. The round bottom was removed from the glove box and the degassed DMAc (7 mL) was slowly added via a syringe. The mixture was allowed to stir at room temperature for 5 minutes and then lowered into a preheated, 30 °C oil bath. The reaction mixture was then and ramped to 120 °C at a rate of 10 °C/5 minutes. The polymerization was allowed to proceed for 14 hours. Then, the reaction was cooled to 90 °C and exposed to air to add an excess amount of palladium scavenger diethylammonium diethyldithiocarbamate, a potassium scavenger 18-crown-6, and 10 mL of chlorobenzene. The mixture was stirred for 1 hour before it was precipitated into 250 mL of methanol. The crude polymer was filtered through a cellulose extraction thimble and subjected to successive Soxhlet extractions with methanol, acetone, hexanes, THF, and finally isolated in chloroform. The chloroform solution was concentrated under reduced pressure, precipitated into methanol, collected via vacuum filtration, and dried under vacuum for 24 hours. The polymer collected from the chloroform Soxhlet fraction was a dark purple solid (670 mg, 83%). Mn: 38.4 kg/mol, Mw: 69.1 kg/mol, Đ: 1.8 (in chloroform at 40 °C vs. polystyrene).

Figure S49. 1H-NMR spectrum (500 MHz) of ProDOT(OE3)-co-ProDOT(Oct) in CDCl3.

Figure S50. Size exclusion chromatogram of ProDOT(OE3)-co-ProDOT(Oct) (40 °C CHCl3, calibrated versus polystyrene).

Synthesis Details of PyDPP derivatives

General methods:

Low resolution MALDI-TOF was performed on a Bruker Autoflex Speed LRF using trans-2-[3-(4-tert-Butylphenyl)-2-methyl-2-propenylidene]malononitrile (DCTB) as the matrix. The samples were dissolved in chloroform with concentration of about 1mg/90µL for characterization.

Elemental analysis was performed by the University of Illinois Microanalysis Laboratory with Exeter Analytical - Model CE440 CHN Analyzer.

NMR were recorded in CDCl3 at room temperature on Varian VXR 500 with Unity Inova console and Carver B500 Bruker Avance III HD NMR Spectrometer.

Gel Permeation Chromatography (GPC) for polymer and oligomers were characterized with Tosoh HLC8321 GPC/HT system in 1,2,4-trichlorobenzene at 140 °C (calibrated vs. polystyrene).

All commercially available chemicals are used as received. Pd2(dba)3 (98%), P(o-tolyl)3 (98%), 11-(bromomethyl)tricosane (97%), 9-(bromomethyl)nonadecane (97%), 5,5′-bis(trimethylstannyl)-2,2′-bithiophene (97%), 3,3'-Difluoro-5,5'-bis(trimethylstannyl)-2,2'-bithiophene (97%), and K2CO3 (99%) were purchased from Ambeed. 18-Crown-6 (98%) was ordered from AA Blocks. Anhydrous toluene, chloroform, dimethylformamide, and tetrahydrofuran were purchased from Sigma Aldrich. ACS-grade extraction and chromatography solvents were purchased from Fisher Scientific.

- Synthesis of PyDPP-2T (C8C10) polymer

The C8C10PyDPP-2T polymer was synthesized accroding to literature23  (2). Elemental analysis calculated for C64H92N4O2S2: C, 75.85%; H, 9.15%; N, 5.53%; found: C, 75.50%; H, 9.03%; N, 5.55%. GPC: Mn = 14.4 kDa, PDI = 3.30.

Figure S51. Size exclusion chromatograms of PyDPP-2T polymer in 1,2,4-trichlorobenzen at 140 oC (calibrated vs. polystyrene). The average molecular (Mn) weight was determined to be 14.4 kg/mol with PDI= 3.30.

- Synthesis of PyDPP-2T2F polymer

C8C10PyDPPBr (100.9 mg, 0.1mmol), 3,3'-Difluoro-5,5'-bis(trimethylstannyl)-2,2'-bithiophene (52.8 mg, 0.1 mmol), Pd2(dba)3 CHCl3 (5.0 mg, 5 mol%.), P(o-tol)3 (4.6 mg, 15 mol%) were added to a Schlenk tube. The tube was purged three times, then toluene (10 mL) was injected, and the mixture was stirred at 130 °C for 72 h. After cooling to room temperature, diethylammonium diethyldithiocarbamate (as palladium scavenger 50 mg) was added, and the mixture was stirred for 3 h to before precipitation into methanol (100 mL). The precipitate was purified via Soxhlet extraction for methanol, acetone and was collected with chloroform. The chloroform solution was then concentrated by evaporation and precipitated into methanol (200 mL) and filtered off as a dark solid (94 mg, yield 90%). The C8C10PyDPP-2T2F polymer was synthesized accroding to literature (2). Elemental analysis calculated for C64H90N4O2S2F2: C, 73.24%; H, 8.64%; N, 5.34%; found: C, 73.19%; H, 8.48%; N, 5.57%. GPC: Mn = 18.5 kDa, PDI = 4.50.

Figure S52. Size exclusion chromatograms of PyDPP-2T2F polymer in 1,2,4-trichlorobenzen at 140 oC (calibrated vs. polystyrene). The average molecular (Mn) weight was determined to be 18.5kg/mol with PDI= 4.50.

- Synthesis of PyDPP-2T (C10C12) Polymer

C10C12PyDPPBr: 18-Crown-6 (0.158 g, 0.6 mmol) and PyDPPBr (0.996 g, 2 mmol) were added to a round bottom flask with 40 mL anhydrous DMF. The mixture was stirred at 90 oC under nitrogen for 30 min. K2CO3 (0.828 g, 6 mmol) and 11-(bromomethyl)tricosane (2.17 g, 5.2 mmol) were added to the mixture and stirred at 90 oC for 24 h. After cooling to room temperature, water (20 mL) and hexanes (30 mL) were added to the flask. The reaction mixture was filtered, the liquid was extracted with hexanes (50 mL × 3) and dried over Na2SO4. After removed the solvent, the raw product was isolated by columns chromatography on silica gel with a mixture of DCM: hexanes = 5: 5. The product was recrystallized with methanol, obtained as a red solid (0.168 g, 75%). 1H NMR (500 MHz, CDCl3) δ 8.93 (d, J = 8.6 Hz, 2H), 8.74 (d, J = 2.3 Hz, 2H), 8.01 (dd, J = 8.6, 2.4 Hz, 2H), 4.28 (d, J = 7.3 Hz, 4H), 1.61 (q, J = 6.4 Hz, 2H), 1.31 – 1.11 (m, 80H), 0.87 (m, 12H). 13C NMR (126 MHz, CDCl3) δ 162.63, 150.25, 146.20, 145.11, 139.84, 128.61, 122.73, 111.57, 46.44, 38.37, 32.08, 31.60, 30.16, 29.86, 29.84, 29.81, 29.77, 29.52, 26.53, 22.85, 14.28. MALDI-TOF calculated for C64H104Br2N4O2 M+: 1120.6501, found: 1120.832. Elemental analysis calculated for C64H104Br2N4O2: C, 68.55%; H, 9.35%; N, 5.00%; found: 68.79%; H, 9.49%; N, 5.05%.

Figure S53. 1H NMR spectrum of C10C12PyDPPBr at room temperature in CDCl3.

Figure S54. 13C NMR spectrum of C10C12PyDPPBr at room temperature in CDCl3.

Figure S55. MALDI-TOF spectrum of C10C12PyDPPBr.

PyDPP-2T (C10C12) polymer: C10C12PyDPPBr (112.1 mg, 0.1mmol), 5,5′-bis(trimethylstannyl)-2,2′-bithiophene (49.2 mg, 0.1 mmol), Pd2(dba)3 CHCl3 (5.0 mg, 5 mol%.), P(o-tol)3 (4.6 mg, 15 mol%) were added to a Schlenk tube. The tube was purged three times, then toluene (10 mL) was injected, and the mixture was stirred at 130 °C for 72 h. After cooling to room temperature, diethylammonium diethyldithiocarbamate (as palladium scavenger 50 mg) was added, and the mixture was stirred for 3 h before precipitation into methanol (100 mL). The precipitate was purified via Soxhlet extraction for methanol, acetone and was collected with chloroform. The chloroform solution was then concentrated by evaporation and precipitated into methanol (200 mL) and filtered off as a dark solid ( 95 mg, yield 84%). Elemental analysis calculated for C72H108N4O2S2: C, 76.82%; H, 9.67%; N, 4.98%; found: C, 76.39%; H, 9.49%; N, 5.03%. GPC: Mn = 56.7 kDa, PDI = 3.30.

Figure S56. Size exclusion chromatograms of C10C12PyDPP-2T polymer in 1,2,4-trichlorobenzene at 140 oC (calibrated vs. polystyrene). The average molecular (Mn) weight was determined to be 56.7 kg/mol with PDI = 3.30.

Section S2. Details on features considered in this study.

Figure S57. Complete list of the 77 features considered in this study. Features shown in black are the 41 retained after correlation-based feature pruning and used to train the ML models. Features shown in gray are the 36 excluded because of their high correlations with retained features.

A total of 77 features were considered in this study. Among them, Temperature, Concentration_mg_mL, Mw_Mn, Mw_Mw, and PDI were obtained directly from experimental measurements. MolWt_monomer was calculated from the monomer structure, whereas one-hot-encoded family features were generated from the assigned polymer families. Backbone (BB) and side-chain (SC) structural descriptors were manually derived from the polymer structures, following the definitions described in the previous work.5 Additional molecular-structure descriptors, shape descriptors, and partition coefficients were calculated using RDKit. FASTSOLV solubility descriptors were predicted using the FASTSOLV model,24 and COSMO-RS solvation free energies were calculated using ORCA 6.0.25 Additional details of the feature-generation workflow are provided in an example Jupyter notebook included in the GitHub (https://github.com/TheJacksonLab/ChiralML).

Section S3. Selection of machine-learning framework.

To identify a suitable machine-learning framework for the present task, we compared random forest (RF), support vector machine (SVM), and a fully connected neural network (NN) using the initial processed ML dataset. For the classification task, systems with (g≥0.001) were labeled as positive cases. For the regression task, only positive cases were included, and (log10g) was used as the prediction target.

The hyperparameters of each framework were optimized using Optuna26 over 80 trials. During cross-validation, all measurements associated with the same polymer–solvent pair were assigned to the same fold. This grouping prevented information leakage between measurements of the same polymer–solvent pair collected at different concentrations or temperatures. Five-fold grouped cross-validation was used during hyperparameter optimization. Average precision (AP) was selected as the primary classification metric because it summarizes precision–recall performance across thresholds and is well suited to imbalanced datasets. Root-mean-square error (RMSE) was used as the primary regression metric.

After hyperparameter optimization, the best-performing configuration of each framework was evaluated using 20 repeats of grouped five-fold out-of-fold (OOF) cross-validation. Different random group assignments were used for each repeat, while measurements from the same polymer–solvent pair remained within a single fold. Model performance is reported as the mean and standard deviation across the 20 repeats in Table S2 and Table S3.

Table S2. Comparison between ML frameworks on the classification task.

|  | OOF AP | OOF Precision@0.5 | Baseline Positive Rate |
| --- | --- | --- | --- |
| Random Forest (RF) | 0.781 ± 0.019 | 0.738 ± 0.019 | 0.360 |
| Supporting Vector Machine (SVM) | 0.751 ± 0.018 | 0.715 ± 0.023 |  |
| Neural Network (NN) | 0.781 ± 0.027 | 0.702 ± 0.032 |  |

Table S3. Comparison between ML frameworks on the regression task.

|  | OOF RMSE | OOF R2 | Baseline Mean Value RMSE |
| --- | --- | --- | --- |
| Random Forest (RF) | 0.568 ± 0.008 | -0.005 ± 0.028 | 0.566 |
| Supporting Vector Machine (SVM) | 0.563 ± 0.011 | 0.011 ± 0.038 |  |
| Neural Network (NN) | 0.647 ± 0.038 | -0.309 ± 0.155 |  |

AP summarizes the precision–recall curve as a weighted average of precision across classification thresholds, with the increase in recall at each threshold serving as the weight:

As shown in Table S2, RF exhibited the highest classification performance among the three frameworks and was therefore selected for subsequent classification and interpretation analyses. The final RF classifier used 1,100 trees, a maximum tree depth of 12, a minimum of two samples per leaf, a minimum of two samples required to split an internal node, 50% of the features considered at each split, balanced class weights, and bootstrap sampling.

In contrast, all three regression frameworks showed limited predictive performance for the magnitude of chirality, as indicated by their low or negative grouped OOF coefficient of determination, R2, values in Table S3.

These results suggest that the current features contain sufficient information to distinguish whether detectable chirality emerges but do not adequately capture the continuous magnitude of (g). This limitation may arise from the smaller number of positive training examples, experimental variability in the measured g-factors, and lack of relevant molecular or assembly-level information that is not represented by the current feature set. Consequently, the RF classification model, rather than the regression models, was used as the primary predictive framework in this study.

Figure S58. SHAP importance and importance-rank stability of the top 20 features for the RF classification model trained on the full polymer dataset. The left panel shows the mean absolute SHAP value of each feature averaged over 20 random seeds, with error bars indicating the seed-to-seed standard deviation. The right panel shows the corresponding mean SHAP importance rank, where a lower rank indicates greater importance, with error bars indicating the seed-to-seed standard deviation in rank. Features are colored according to their mean directional correlation with the model output, with red indicating a positive association and blue indicating a negative association.

Section S4. Family related RF classification model performance.

Table S4. Results of leave-one-family-out evaluation.

| Family Name | Data Point Number | Positive Rate | AP | Precision @0.5 | Recall @0.5 |
| --- | --- | --- | --- | --- | --- |
| Thiophene | 248 | 0.129 | 0.101 | 0.000 | 0.000 |
| NDI | 143 | 0.469 | 0.754 | 0.671 | 0.634 |
| II | 130 | 0.546 | 0.872 | 0.578 | 0.803 |
| Qx | 69 | 0.232 | 0.326 | 0.320 | 0.550 |
| DPP | 65 | 0.723 | 0.899 | 0.963 | 0.551 |
| DOT | 37 | 0.486 | 0.641 | 0.500 | 0.006 |
| TPT | 36 | 0.000 | NaN | 0.000 | NaN |
| BDT | 20 | 0.250 | 0.363 | NaN | 0.000 |
| Ladder | 16 | 0.438 | 0.292 | NaN | 0.000 |
| Polyfluorene | 6 | 1.000 | 1.000 | NaN | 0.000 |
| IDT | 3 | 0.667 | 1.000 | NaN | 0.000 |

The RF classifier was primarily designed to predict untested solvent and processing conditions for polymers represented in the training dataset, rather than to extrapolate to entirely unseen polymer chemistries. Nevertheless, we assessed the cross-family transferability of the modeling framework using a leave-one-family-out analysis. In each iteration, all data points belonging to one polymer family were withheld as the test set, and an RF classifier was trained using data from all remaining families. Model performance was evaluated using average precision (AP), with the positive fraction of each held-out family used as the corresponding random-ranking baseline. Predictions at a RF prediction score threshold of 0.5 were also examined to assess threshold-dependent classification performance.

The concatenated leave-one-family-out predictions yielded an overall AP of 0.614, compared with an overall positive-rate baseline of 0.351, indicating that certain predictive information is transferable across polymer families. For the held-out NDI, II, Qx, DPP, and DOT families, the AP values exceeded their respective positive-rate baselines. The strongest relative improvements were observed for NDI and II, followed by DPP and DOT, whereas the improvement for Qx was more modest. These results indicate that the descriptors learned from the remaining families retain some ability to rank positive and negative cases within these held-out families.

However, an AP above the positive-rate baseline does not necessarily imply that the RF prediction scores are well calibrated for the unseen family. For example, the DOT family exhibited an AP of 0.641, compared with a positive rate of 0.486, but only a few of its data points were classified as positive at a RF prediction score threshold of 0.5. Thus, the model retained useful ranking information for this family, while systematically assigning RF prediction scores below 0.5. Similar family-dependent differences between ranking performance and threshold-based classification indicate that a decision threshold established using the training families may not transfer directly to a structurally distinct family.

For the Thiophene and Ladder groups, the AP values were lower than their positive-rate baselines, indicating little or no useful cross-family ranking performance. In particular, the Thiophene family contained a relatively low positive fraction and occupied a substantial portion of the dataset, yet its positive cases were not successfully distinguished by a model trained without thiophene-based polymers. The Ladder category also showed poor transferability, which is unsurprising because it shows very different structure compared to other polymers.

The TPT family contained no positive data points; therefore, AP and recall were undefined for this held-out set. At a RF prediction score threshold of 0.5, the model incorrectly classified 9 of 36 TPT data points as positive. These false-positive predictions further demonstrate that models trained on the remaining families cannot reliably establish the absolute classification boundary for these unseen chemical families.

Overall, the leave-one-family-out analysis demonstrates partial but strongly family-dependent transferability. The current descriptors capture relationships that generalize to several polymer families, but the model does not consistently extrapolate across all backbone and side-chain chemistries, and its RF prediction score calibration can shift substantially for an unseen family. Therefore, predictions for polymers outside the chemical domain represented in the training dataset should be treated as exploratory and require experimental validation or model updating with representative data from the new polymer family.

We also performed leave-one-polymer-out and leave-one-solvent-out analyses. Pooling the held-out predictions yielded overall APs of 0.671 and 0.680, respectively, supporting the model’s ability to generalize to unseen polymers within represented polymer families. The results of ten most frequent solvents in the dataset are shown in Table S5, the obvious larger AP comparing to baseline indicates the good performance to unseen solvents.

Table S5. Results of leave-one-solvent-out evaluation.

| Solvent Name | Data Point Number | Positive Rate | AP | Precision @0.5 | Recall @0.5 |
| --- | --- | --- | --- | --- | --- |
| Chlorobenzene | 206 | 0.510 | 0.845 | 0.942 | 0.463 |
| Chloroform | 113 | 0.478 | 0.735 | 0.960 | 0.444 |
| o-Dichlorobenzene o-Dichlorobenzene. | 83 | 0.422 | 0.934 | 0.888 | 0.766 |
| Anisole | 72 | 0.125 | 0.389 | 0.357 | 0.556 |
| Toluene | 46 | 0.348 | 0.884 | 0.765 | 0.813 |
| p-Xylene | 43 | 0.256 | 0.731 | 0.786 | 1.000 |
| PGMEA | 39 | 0.077 | 1.000 | 0.247 | 1.000 |

Table S6. Performance of the RF classification models on the total dataset and family-specific subsets.

| ML Dataset | Baseline Positive Rate | OOF AP | OOF Precision@0.5 |
| --- | --- | --- | --- |
| All Polymer | 0.351 | 0.798 ± 0.017 | 0.733 ± 0.018 |
| Thiophene Family | 0.127 | 0.511 ± 0.066 | 0.503 ± 0.074 |
| NDI Family | 0.469 | 0.848 ± 0.019 | 0.804 ± 0.035 |

To examine whether the factors governing chiral emergence differ among polymer families, we separately trained RF classification models on the Thiophene and NDI subsets and subsequently performed family-specific SHAP analyses. The predictive performance of these models is summarized in Table S6. For these family-specific datasets, the OOF AP was substantially higher than the corresponding positive-rate baseline, indicating that the models captured nonrandom relationships between the input features and the classification labels within each family. The NDI model showed particularly strong predictive performance, whereas the Thiophene model exhibited lower absolute performance but still substantially exceeded its low positive-rate baseline. These results support the use of SHAP analysis to interpret the feature–prediction relationships learned by the family-specific RF models, while recognizing that the resulting feature importance reflects patterns within each individual family rather than universally transferable design rules.

Section S5. Solubility-based evidence supporting the proposed mechanism of chiral LLC formation.

Figure S59. Distributions of negative log∣g∣<-3 and positive log∣g∣≥-3 cases with respect to the polymer molecular weight used in the SHAP analysis of RF classification models trained on full processed ML dataset. Achiral cases dominate below approximately 104, chiral cases are most prevalent around this molecular-weight range, and the relative fraction of achiral cases increases again at higher molecular weights.

Figure S60. Experimental distribution of assembly outcome in the two-dimensional space defined by the FASTSOLV-derived monomer and backbone solubility descriptors. Results are shown for the complete dataset and individual polymer families. The number of experimental data points in full processed ML dataset are indicated by n in the title of each panel.

Figure S61. Relationship between monomer FASTSOLV and assembly outcome. Assembly outcomes are grouped into five monomer FASTSOLV ranges and shown as binned fractions of strongly chiral (red), weakly chiral (light red), isotropic (light blue), and aggregated (blue) outcomes. The number above each bar indicates the total number of polymer–solvent–temperature conditions within each FASTSOLV range. At higher monomer FASTSOLV values, isotropic outcomes become increasingly prevalent, whereas chiral outcomes are most enriched within an intermediate FASTSOLV regime.

Figure S62. RF prediction score of log⁡10∣g∣≥-3 in the two-dimensional space defined by the FASTSOLV-derived monomer and backbone solubility descriptors for the expanded polymer–solvent dataset. The number of generated polymer–solvent pairs (number of polymers × 44 solvents) are indicated by n in the title of each panel.

The experimental and RF-predicted distributions with respect to the solubility-related descriptors are summarized in Figures S60-S62.

The experimental data were further projected onto the two-dimensional plane defined by the FASTSOLV-derived monomer and backbone solubility descriptors (Figure S60). Across the full dataset, positive cases and larger (g) values occur primarily within an intermediate region of this plane.

To examine the model response over a broader polymer–solvent chemical space, we plotted RF prediction scores for the expanded set of polymer–solvent combinations (Figure S62). The RF model generally assigns higher RF prediction scores of (log10g≥-3) within intermediate solubility regimes, while lower RF prediction scores are observed toward the extreme high- and low-solubility regions.

Taken together, these observations are consistent with a balanced-solvation hypothesis for chiral LLC formation. An intermediate solvent regime may provide a balance between solubilization and intermolecular association that facilitates chiral mesophase formation. The present analysis identifies a statistical association consistent with the hypothesis but does not by itself establish a causal mechanism.

The FASTSOLV descriptors should nevertheless be interpreted with caution. FASTSOLV was developed primarily to predict the solubility of small organic molecules24 and does not explicitly account for polymer molecular weight, chain conformation, aggregation, crystallinity, or polymer-specific solution thermodynamics. Here, FASTSOLV predictions for the monomer, backbone, and side-chain fragments are therefore used as proxy descriptors of relative polymer–solvent compatibility rather than as quantitative predictions of whole-polymer solubility. Furthermore, the RF prediction score maps in Figure S62 are generated by an RF model that uses these FASTSOLV descriptors as input features and should therefore be viewed as visualizations of the relationships learned by the model, rather than as independent validation of the solubility hypothesis. Predictions in sparsely represented or extrapolative regions of the descriptor space remain uncertain. Polymer-specific solvation models and additional experimental measurements will be required to quantitatively resolve how solvent quality governs chiral LLC formation.

Section S6. Additional results for feature analysis.

Figure S63. Experimentally observed assembly outcomes plotted as a function of normalized side-chain content. Each condition is classified as strongly chiral, weakly chiral, isotropic, or aggregated outcomes.

Figure S64. SHAP importance and importance-rank stability of the top 20 features for the RF classification model trained on the thiophene family subset. All quantities, error bars, and color conventions are defined as in Figure S58.

Figure S65. SHAP importance and importance-rank stability of the top 20 features for the RF classification model trained on the NDI family subset. All quantities, error bars, and color conventions are defined as in Figure S58.

Figure S66. Concentration-resolved experimental assembly outcomes for NDI-family polymers, including p(C3NDI-T), p(C6NDI-T), N2200-OE, and N2200 with six different molecular weights. Colors indicate strongly chiral (red), weakly chiral (light red), isotropic (light blue), and aggregated (blue) outcomes, while marker shapes distinguish solvent conditions. Vertical segments indicate conditions for which the concentration was reported as a range. The shaded region highlights the N2200 molecular-weight series.

Reference

(1)	Yao, Y.; Ugras, T. J.; Meyer, T.; Dykes, M.; Wang, D.; Arbe, A.; Bals, S.; Kahr, B.; Robinson, R. D. Extracting Pure Circular Dichroism from Hierarchically Structured CdS Magic Cluster Films. ACS Nano 2022, 16 (12), 20457–20469. https://doi.org/10.1021/acsnano.2c06730

(2)	Yin, W.; Dong, Y.; Zhang, R.; Zhao, B.; Deng, J. Anisotropic Artifacts Coupled with Light-Scattering Generating “Non-Reciprocal-Like” CD/CPL Signals in Polyurethane Films. Macromolecules 2025, 58 (18), 9660–9671. https://doi.org/10.1021/acs.macromol.5c00577

(3)	Jeon, S.; Neu, J. S.; Ahn, N.; Senlik, A.; Chen, Y. C.; Fernando, P. S.; Bairagya, P.; Prasad, C. K.; Baek, J. M.; You, W.; Diao, Y. Solvent-Guided Chiral Assemblies and Chemical Doping of OEG-Functionalized Conjugated Polymers. Advanced Materials 2026. https://doi.org/10.1002/adma.74130

(4)	Kashani, S.; Neu, J.; Kwon, S. J.; Song, R.; Chen, Z.; Trapier, T.; Gkoupidenis, P.; Ginger, D.; You, W.; Michels, J. J.; Ade, H. Thermodynamic Limits to Molecular Doping in Conjugated Polymers: A Perspective on Phase Behavior and Miscibility. Advanced Materials 2026. https://doi.org/10.1002/adma.202522989

(5)	Xu, Z.; Wang, Z.; Zhang, R.; Verma, A.; Neu, J. S.; Bairagya, P.; Jeon, S.; Damron, A. M.; Rinehart, J. M.; Wagner, J. S.; Sabury, S.; Luo, X.; Österholm, A. M.; Mei, J.; Moore, J. S.; You, W.; Reynolds, J. R.; Jackson, N. E.; Diao, Y. Ubiquitous Chiral Symmetry Breaking of Conjugated Polymers via Liquid–Liquid Phase Separation. J. Am. Chem. Soc. 2025, 147 (37), 33530–33544. https://doi.org/10.1021/jacs.5c07995

(6)	Rinehart, J. M.; Xu, Z.; Wang, Z.; Österholm, A. M.; Flagg, L. Q.; Richter, L. J.; Snyder, C. R.; Diao, Y.; Reynolds, J. R. Impact of Side-Chain Polarity and Symmetry on the Structure and Properties of Acyclic Dioxythiophene Polymers. Chemistry of Materials 2025, 37 (13), 4593–4606. https://doi.org/10.1021/acs.chemmater.4c03394

(7)	Griggs, S.; Marks, A.; Meli, D.; Rebetez, G.; Bardagot, O.; Paulsen, B. D.; Chen, H.; Weaver, K.; Nugraha, M. I.; Schafer, E. A.; Tropp, J.; Aitchison, C. M.; Anthopoulos, T. D.; Banerji, N.; Rivnay, J.; McCulloch, I. The Effect of Residual Palladium on the Performance of Organic Electrochemical Transistors. Nature Communications 2022, 13 (1). https://doi.org/10.1038/s41467-022-35573-y

(8)	Xu, Z.; Park, K. S.; Kwok, J. J.; Lin, O.; Patel, B. B.; Kafle, P.; Davies, D. W.; Chen, Q.; Diao, Y. Not All Aggregates Are Made the Same: Distinct Structures of Solution Aggregates Drastically Modulate Assembly Pathways, Morphology, and Electronic Properties of Conjugated Polymers. Advanced Materials 2022, 34 (32). https://doi.org/10.1002/adma.202203055

(9)	Park, K. S.; Luo, X.; Kwok, J. J.; Khasbaatar, A.; Mei, J.; Diao, Y. Subtle Molecular Changes Largely Modulate Chiral Helical Assemblies of Achiral Conjugated Polymers by Tuning Solution-State Aggregation. ACS Cent. Sci. 2023, 9 (11), 2096–2107. https://doi.org/10.1021/acscentsci.3c00775

(10)	Xu, Z.; Saiev, S.; Qian, P.; Nabei, Y.; Wang, Z.; Rinehart, J. M.; Österholm, A. M.; Jones, A. L.; Lee, J.-H.; Hwang, C.; Wang, S.; Sun, R.; Shin, D.; Jeon, S.; Elangovan, K. E.; Vura-Weis, J.; Coropceanu, V.; Rodríguez-López, J.; Reynolds, J. R.; Sun, D.; Brédas, J.-L.; Diao, Y. Supramolecular Chirality Largely Modulates Chemical Doping of Conjugated Polymers. Nat. Commun. 2025, 16 (1), 8381. https://doi.org/10.1038/s41467-025-62915-3

(11)	Kim, F. S.; Park, C. H.; Na, Y.; Jenekhe, S. A. Effects of Ladder Structure on the Electronic Properties and Field-Effect Transistor Performance of Poly(Benzobisimidazobenzophenanthroline). Org. Electron. 2019, 69, 301–307. https://doi.org/10.1016/j.orgel.2019.03.049

(12)	Mueller, C. J.; Singh, C. R.; Thelakkat, M. EDOT-Diketopyrrolopyrrole Copolymers for High Bulk Hole Mobility and near Infrared Absorption. J. Polym. Sci. B Polym. Phys. 2016, 54 (6), 639–648. https://doi.org/10.1002/polb.23955

(13)	Yamakawa, S.; Wada, K.; Hidaka, M.; Hanasaki, T.; Akagi, K. Chiral Liquid-Crystalline Ionic Liquid Systems Useful for Electrochemical Polymerization That Affords Helical Conjugated Polymers. Adv. Funct. Mater. 2019, 29 (12). https://doi.org/10.1002/adfm.201806592

(14)	Murugan, P.; Raghavendra, V.; Chithiravel, S.; Krishnamoorthy, K.; Mandal, A. B.; Subramanian, V.; Samanta, D. Experimental and Theoretical Investigations of Different Diketopyrrolopyrrole-Based Polymers. ACS Omega 2018, 3 (9), 11710–11717. https://doi.org/10.1021/acsomega.8b01132

(15)	Kosco, J.; Gonzalez-Carrero, S.; Howells, C. T.; Zhang, W.; Moser, M.; Sheelamanthula, R.; Zhao, L.; Willner, B.; Hidalgo, T. C.; Faber, H.; Purushothaman, B.; Sachs, M.; Cha, H.; Sougrat, R.; Anthopoulos, T. D.; Inal, S.; Durrant, J. R.; McCulloch, I. Oligoethylene Glycol Side Chains Increase Charge Generation in Organic Semiconductor Nanoparticles for Enhanced Photocatalytic Hydrogen Evolution. Advanced Materials 2022, 34 (2105007).

(16)	Song, I. Y.; Park, S. H.; Lim, J.; Kwon, Y. S.; Park, T. A Novel Hole Transport Material for Iodine-Free Solid State Dye-Sensitized Solar Cells. Chemical Communications 2011, 47 (37), 10395–10397. https://doi.org/10.1039/c1cc13376d

(17)	Hallani, R. K.; Paulsen, B. D.; Petty, A. J.; Sheelamanthula, R.; Moser, M.; Thorley, K. J.; Sohn, W.; Rashid, R. B.; Savva, A.; Moro, S.; Parker, J. P.; Drury, O.; Alsufyani, M.; Neophytou, M.; Kosco, J.; Inal, S.; Costantini, G.; Rivnay, J.; McCulloch, I. Regiochemistry-Driven Organic Electrochemical Transistor Performance Enhancement in Ethylene Glycol-Functionalized Polythiophenes. J. Am. Chem. Soc. 2021, 143 (29), 11007–11018. https://doi.org/10.1021/jacs.1c03516

(18)	Halaksa, R.; Kim, J. H.; Thorley, K. J.; Gilhooly-Finn, P. A.; Ahn, H.; Savva, A.; Yoon, M. H.; Nielsen, C. B. The Influence of Regiochemistry on the Performance of Organic Mixed Ionic and Electronic Conductors. Angew. Chem. Int. Ed. 2023, 62 (29). https://doi.org/10.1002/anie.202304390

(19)	Zeng, D.; Tahar-Djebbar, I.; Xiao, Y.; Kameche, F.; Kayunkid, N.; Brinkmann, M.; Guillon, D.; Heinrich, B.; Donnio, B.; Ivanov, D. A.; Lacaze, E.; Kreher, D.; Mathevet, F.; Attias, A. J. Intertwined Lamello-Columnar Coassemblies in Liquid-Crystalline Side-Chain π-Conjugated Polymers: Toward a New Class of Nanostructured Supramolecular Organic Semiconductors. Macromolecules 2014, 47 (5), 1715–1731. https://doi.org/10.1021/ma4020356

(20)	Sabury, S.; Xu, Z.; Saiev, S.; Davies, D.; Österholm, A. M.; Rinehart, J. M.; Mirhosseini, M.; Tong, B.; Kim, S.; Correa-Baena, J. P.; Coropceanu, V.; Jurchescu, O. D.; Brédas, J. L.; Diao, Y.; Reynolds, J. R. Non-Covalent Planarizing Interactions Yield Highly Ordered and Thermotropic Liquid Crystalline Conjugated Polymers. Mater. Horiz. 2024, 11 (14), 3352–3363. https://doi.org/10.1039/d3mh01974h

(21)	Advincula, A. A.; Jones, A. L.; Thorley, K. J.; Österholm, A. M.; Ponder, J. F.; Reynolds, J. R. Probing Comonomer Selection Effects on Dioxythiophene-Based Aqueous-Compatible Polymers for Redox Applications. Chemistry of Materials 2022, 34 (10), 4633–4645. https://doi.org/10.1021/acs.chemmater.2c00511

(22)	Attia, L.; Burns, J. W.; Doyle, P. S.; Green, W. H. Data-Driven Organic Solubility Prediction at the Limit of Aleatoric Uncertainty. Nature Communications 2025, 16 (1). https://doi.org/10.1038/s41467-025-62717-7

(23)	Neese, F. Software Update: The ORCA Program System—Version 6.0. Wiley Interdisciplinary Reviews: Computational Molecular Science. John Wiley and Sons Inc March 1, 2025. https://doi.org/10.1002/wcms.70019

(24)	Akiba, T.; Sano, S.; Yanase, T.; Ohta, T.; Koyama, M. Optuna: A Next-Generation Hyperparameter Optimization Framework. In Proceedings of the ACM SIGKDD International Conference on Knowledge Discovery and Data Mining; Association for Computing Machinery, 2019; pp 2623–2631. https://doi.org/10.1145/3292500.3330701